## Slide 1
PART NUMBER: 1N5822DIE2HR, 1N5822DIE2S
DIE REFERENCE: NOT MARKED
Technological and mechanical characteristics of chip | 
Substrate | Silicon
Wafer fab. | AMK 5” / AMK 6”
Die size | X = 1690 µm Y= 1690 µm
Thickness | 280µm +/- 20µm
Top metallization | TIW-Ni-Al 0.1-0.08-10µm
Back metallization | Ti-Ni-Au
Top passivation | PIX (5”) / PROBIMIDE (6”)
Pad size | X = 1500 µm Y= 1500 µm
Scribing | Saw
Back side contact | Cathode
Top side contact | Anode
Die orientation
The die corner highlighted in red in the die layout
drawing above is positioned in the waffle pack as
indicated in the schematics beside.
Waffle pack
Entegris H20-070-24-62C02