## Slide 1
PART NUMBER: 1N6642DIE2HR, 1N6642DIE2S
DIE REFERENCE: NOT MARKED
Technological and mechanical characteristics of chip | 
Substrate | Silicon
Wafer fab. | Tours 6”
Die size | X = 390 µm Y= 390 µm
Thickness | 235µm +/- 20µm
Top metallization | Al 3µm
Back metallization | Ti-Ni-Au
Top passivation | PROBIMIDE
Pad size | X = 110 µm Y= 110 µm
Scribing | Saw
Back side contact | Cathode
Top side contact | Anode
Die orientation
The die corner highlighted in red in the die layout
drawing above is positioned in the waffle pack as
indicated in the schematics beside.
Waffle pack
Entegris H20-018-62C02