## Slide 1
PART NUMBER: 4014EDIE2S, 4014BEDIE2HR
DIE REFERENCE: C4144 – P14B – 800A
1
15
14
13
12
10
8
VSS
7
5
4
3
2
VDD
16
Technological and mechanical characteristics of chip | 
Substrate | Silicon
Wafer fab. | Singapour
Die size | 81 X 72mils²
Thickness | 525 ± 25 µm
Top metallization | Al/Si 1% (1.1 ± 0.1 µm)
Back metallization | Bare Silicon
Top passivation | P. Vapox 8000 ± 1600 Å
Pad size | 90 X 90 µm
Scribing | Saw
Back side contact | VDD
Die orientation
The die corner highlighted in red in the die layout
drawing above is positioned in the waffle pack as
indicated in the schematics beside.
Waffle pack
Entegris H20-090-24-62C02
ST logo
Pad numbers are those of FP, DIP and SO package
6
5
9
11