## Slide 1
PART NUMBER: STRH12P10
DIE REFERENCE: I4681
Technological and mechanical characteristics of chip | 
Substrate | Silicon
Wafer fab. | Catania 6”
Die size | X = 2922 µm Y= 2440 µm
Thickness | 280µm +/- 20µm
Top metallization | Al/Si
Back metallization | Cr/Ni/Ag
Top passivation | Nitride
Gate Pad size | X = 344 µm Y= 460 µm
Scribing | Saw
Back side contact | Drain
Die orientation
The die corner highlighted in red in the die layout
drawing above is positioned in the waffle pack as
indicated in the schematics beside.
Waffle pack
Entegris H20-120-24-62C02
Source
Gate