## Slide 1: Radiation Tests of Candidate Memory Devices DDR3 SDRAM and NAND Flash
Martin Herrmann, Kai Grürmann, Fritz Gliem, Hagen Schmidt
ESTEC Technical Officer: Véronique Ferlet-Cavrois (TEC-QEC)
Institut für Datentechnik, TU Braunschweig

## Slide 2: Overview
Part 1: DDR3 SDRAM (M. Herrmann)
  Test bed
  SEE tests
    SEL
    Software conditioning
    Hard SEUs
    Hard SEU annealing
  TID tests
    Band error pattern
    Error density
    Temperature dependence
    Annealing
    Idle current
Part 2: NAND Flash (K. Grürmann)

## Slide 3: Test bed – head station (SEE)
Water cooler
Custom
SODIMM
ZIF socket
DDR3 device
(opened)
FPGA
(Xilinx Virtex6)
Power switching

## Slide 4: Test bed – head station (TID)
SODIMM
Flexible
extension
FPGA
(Xilinx Virtex6)

## Slide 5: Test bed – shielding

## Slide 6: SEE tests
Campaigns:
  3 × RADEF, Jyväskylä
  1 × TAMU, College Station, Texas
Parts:
  2 Gbit: Samsung, Hynix, Micron, Nanya
  4 Gbit: Samsung, Hynix, Elpida

## Slide 7: SEE results – SEL
Setup:
  4 Gbit, Samsung and Hynix, thinned to 200 µm
  80 °C
  107 cm-2 Xenon @ 61.1
  Write/read mode
Result:
  No SEL
  Current returns to original value after irradiation

## Slide 8: SEE results – software conditioning
Elpida: reduces device SEFIs
Samsung: no effect
Chart: LET [MeV cm² / mg]
| 3.2 | 5.5 | 13.9 | 26.3 | 40.9 | 69.7
Elpida (without conditioning) | 9.901e-09 | 6.4576e-08 | 9.1743e-07 | 1.3333e-05 | 8.2192e-06 | 3.6364e-05
Samsung (without conditioning) | 6.7334e-09 | 5.6433e-08 | 2.9817e-07 | 5.8997e-07 | 9.1743e-07 | 1.2034e-06
Elpida (with conditioning) | 9.8039e-09 | 1.0929e-08 | 4.1667e-08 | 3.5714e-07 | 4.0323e-07 | 1.6667e-06
Samsung (with conditioning) | 2.0408e-08 | 4.1885e-08 | 1.2281e-07 | 2.4096e-07 | 5.7692e-07 | 1.6667e-06

## Slide 9: SEE results – hard SEU share
Hard SEUs: can not be removed by rewriting
Chart: LET [MeV cm² / mg]
| 2.2000000000000002 | 4.5 | 12.9 | 25.3 | 39.9 | 68.7
SEU - Samsung | 2.3758e-17 | 2.8056e-14 | 1.9234e-14 | 5.6742e-12 | 6.9815e-12 | 1.0529e-10
SEU - Elpida | 4.2542e-16 | 1.6223e-13 | 3.99e-12 | 6.2942e-13 | 2.1912e-12 | 2.2142e-11
Hard SEU - Samsung | 1.1714e-18 | 2.2579e-16 | 1.0752e-15 | 1.9829e-13 | 1.3594e-13 | 2.2321e-12
Hard SEU - Elpida | 3.2747e-18 | 3.583e-16 | 1.5617e-14 | 7.1072e-15 | 3.9457e-15 | 8.0484e-13
Dummy | 10

## Slide 10: SEE results – hard SEU annealing
Chart: Samsung, 2 Gbit
| 2.7777777777777794E-4 | 8.4166666718924227E-2 | 0.16749999997464735 | 0.25277777778010607 | 0.33416666666071665 | 49.035277777868572 | 356.67222222219476
Neon | 1 | 0.5625 | 0.5 | 0.6875 | 0.8125 | 0.125 | 0
Argon | 1 | 0.73529 | 0.73529 | 0.70588 | 0.029412 | 0
Iron | 1 | 0.94444 | 0.94444 | 0.81481 | 0.77778 | 0.7963 | 0.72222 | 0.018519 | -0.11111
Krypton | 1 | 0.86957 | 0.86232 | 0.89855 | 0.84783 | 0.7971 | 0.80435 | 0.094203 | 0
Xenon | 1 | 0.90057 | 0.88918 | 0.88555 | 0.8581 | 0.83376 | 0.83635 | 0.81668 | 0.28586 | 0.036769
Vacuum
Room temperature

## Slide 11: TID campaigns
Campaigns:
  2 × ESTEC, Noordwijk
Parts:
  In-Situ, 4 Gbit: Samsung
  Unbiased, 4 Gbit: Samsung, Hynix, Elpida
  Unbiased, 2 Gbit: Samsung, Hynix, Micron, Nanya

## Slide 12: TID – band error pattern
DRAM: organized in pages

## Slide 13: TID results – error density
Chart: Samsung, 4 Gbit, in-situ, room temperature
| 1.2857814179733396 | 3.1689603468403229 | 11.37842712784186 | 20.16774891782552 | 23.065104166977104 | 31.775965542532504 | 40.476632484234862 | 49.176096180453904 | 57.876763122156255 | 66.577430063858614 | 75.278097005560966 | 83.977560702711344 | 93.385484308004365 | 100.00174776790664 | 109.89139554277061 | 118.89456845354289 | 127.60879017878321 | 136.36670338548723 | 145.08386784326285 | 153.80103230010721 | 162.51699123159048 | 171.23415568843481 | 179.95132014621052 | 188.66727907583117 | 197.38626705762007 | 204.10714285714297 | 204.33571428526193 | 212.95515267923474 | 221.67503720428795 | 230.37256150878966 | 239.0871374215931 | 247.79725323524323 | 256.50736904889339 | 265.21628031134611 | 273.92519157286728 | 282.63530738744885 | 291.34542320109904 | 300.05553901474929 | 308.76565482839936 | 317.46866493485874 | 326.15890591777861 | 334.84914689976733 | 340.61312074959267 | 340.65966730564844 | 340.68646683823317 | 340.70480335969472 | 342.99827912449831 | 343.6541624153034 | 344.38035684777418 | 345.12427731556824 | 346.37957581924275 | 346.51199581520626 | 346.59704605722794 | 346.75207434548065 | 346.90064312238246 | 347.04167580138892 | 347.17301921267051 | 347.68655041791493 | 348.34326747339225 | 348.9300064826383 | 349.33049622830003 | 349.76005377713585 | 350.50335141830141 | 351.22153090592462 | 351.58911263663322 | 351.750460393727 | 352.22479853406554 | 352.57903571426868 | 352.96117513719935 | 353.37000366207207 | 353.61991071421659 | 354.0226735342294 | 354.39874725230027 | 354.75905013736343 | 354.94708699639887 | 363.61014494299883 | 372.2708454625681 | 380.93274386506528 | 389.59464226849371 | 398.25654067099094 | 406.98362698405975 | 407.83200496062631 | 407.86569940485066 | 408.04981547687203 | 408.06545932590961 | 408.08350992109621 | 408.57087599299842 | 408.59855357185 | 408.60336706414824 | 409.10998710338038 | 409.45294841285795 | 409.7706388887018 | 410.20385317504406 | 410.49386607110495 | 410.84645436517894 | 411.25560119096201 | 411.56727480236441 | 411.97762500029052 | 413.32540277764195 | 413.47221428621555 | 413.92101535014797 | 414.03577331919223 | 414.06087662559008 | 414.12303719203919 | 419.49753542058158 | 419.52263872697944 | 419.57882231567055 | 420.87582644820208 | 420.88060802966362 | 420.89136658981437 | 420.91049291752273 | 420.91766529064631 | 420.92483766376972 | 420.93081464059645 | 420.93679161928588 | 420.94157320074731 | 420.94994097016752 | 420.97384887933731 | 421.08621605765063 | 421.09338843077416 | 421.09697461780161 | 421.10056080482906 | 421.10295159555972 | 421.10653778165573 | 421.1089285723865 | 421.1125147594139 | 421.11490555014461 | 421.11729634087533 | 421.12088252790272 | 421.12207792326808 | 421.12566411029547 | 421.12805490102619 | 421.13164108712226 | 421.13403187878424 | 421.13761806488031 | 421.14239964727307 | 421.14479043800389 | 421.14837662503135 | 421.16630755737418 | 422.41071428571422
DUT 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 2.3283e-10 | 6.9849e-10 | 1.1642e-09 | 1.6298e-09 | 5.5879e-09 | 1.0012e-08 | 7.6834e-09 | 5.4715e-08 | 1.5949e-07 | 3.8161e-07 | 8.3493e-07 | 1.7378e-06 | 0
DUT 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 4.6566e-10 | 1.8626e-09 | 4.191e-09 | 5.1223e-09 | 2.0489e-08 | 4.9127e-08 | 1.0151e-07 | 2.3074e-07 | 4.5868e-07
DUT 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 4.6566e-10 | 4.6566e-10 | 1.397e-09 | 3.2596e-09 | 1.1409e-08 | 1.0943e-08 | 4.0745e-08 | 1.0454e-07 | 2.5658e-07 | 5.4436e-07 | 1.1211e-06
DUT 3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 1.1642e-09 | 1.397e-09 | 4.191e-09 | 1.6531e-08 | 4.4238e-08 | 8.8476e-08 | 1.9162e-07 | 4.3563e-07 | 6.0163e-07 | 1.9108e-06 | 4.3858e-06 | 9.1828e-06 | 1.7938e-05 | 3.3806e-05
DUT 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6566e-10 | 1.397e-09 | 1.8626e-09 | 4.4238e-09 | 1.071e-08 | 1.56e-08 | 4.6566e-08 | 1.1548e-07 | 2.7544e-07 | 5.7509e-07 | 1.1725e-06
DUT 5 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 4.6566e-10 | 1.6298e-09 | 4.191e-09 | 1.234e-08 | 3.5623e-08 | 9.872e-08 | 2.4983e-07 | 6.1817e-07 | 1.3777e-06 | 2.1411e-06 | 5.8927e-06 | 1.2754e-05 | 2.6012e-05 | 4.9738e-05 | 9.154e-05
DUT 6 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 2.3283e-10 | 1.1642e-09 | 3.4925e-09 | 6.7521e-09
DUT 7 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2.3283e-10 | 2.3283e-10 | 4.6566e-10 | 4.6566e-10 | 1.397e-09 | 6.9849e-09 | 2.3516e-08 | 7.0315e-08 | 1.9441e-07 | 5.1362e-07 | 1.22e-06 | 2.7956e-06 | 6.3372e-06 | 2.3574e-05 | 5.5428e-05 | 0.00011077 | 0.00020627 | 0.00034132 | 0

## Slide 14: TID results – temperature dependence
Chart: Samsung, 4 Gbit, unbiased, 422 krad
| 1.5 | 6 | 15.3 | 25.3 | 25.3 | 25.6 | 35.1 | 44.3 | 53.5 | 65 | 73.400000000000006 | 83.1 | 92.7
DUT 0 | 60 | 84 | 180 | 250 | 370 | 350 | 480 | 920 | 1900 | 5400 | 15000 | 42000 | 95000
DUT 1 | 4 | 6 | 16 | 31 | 40 | 38 | 60 | 130 | 260 | 640 | 1400 | 3400 | 8800
DUT 2 | 110 | 170 | 340 | 450 | 720 | 770 | 1100 | 2300 | 5800 | 20000 | 52000 | 130000 | 260000
DUT 3 | 18 | 36 | 68 | 86 | 130 | 150 | 190 | 410 | 860 | 2600 | 7100 | 20000 | 51000
DUT 4 | 64 | 100 | 230 | 330 | 500 | 510 | 740 | 1600 | 4200 | 14000 | 42000 | 100000 | 220000
DUT 5 | 1 | 2 | 10 | 18 | 24 | 23 | 52 | 120 | 260 | 680 | 1600 | 4000 | 11000
DUT 6 | 100 | 140 | 290 | 410 | 630 | 640 | 860 | 2100 | 6100 | 18000 | 53000 | 130000 | 270000
DUT 7 | 93 | 140 | 260 | 380 | 530 | 540 | 780 | 1900 | 4800 | 15000 | 42000 | 100000 | 200000

## Slide 15: TID results – annealing
Chart: Samsung, 4 Gbit, in-situ, 422 krad, room temperature
| 0 | 96 | 114.99999999994181 | 150 | 234.99999999994176 | 316.99999999988353 | 408.99999999994179 | 477
DUT 0 | 1 | 0.078571 | 0.071429 | 0.068571 | 0.065714 | 0.06 | 0.044286 | 0.044286
DUT 1 | 1 | 0.16 | 0.13556 | 0.12222 | 0.12667 | 0.11556 | 0.086667 | 0.086667
DUT 2 | 1 | 0.13131 | 0.11111 | 0.092929 | 0.092929 | 0.078788 | 0.061616 | 0.061616
DUT 3 | 1 | 0.16923 | 0.12692 | 0.10769 | 0.092308 | 0.073077 | 0.05 | 0.05
DUT 4 | 1 | 0.13924 | 0.10886 | 0.091139 | 0.089873 | 0.070886 | 0.055696 | 0.055696
DUT 5 | 1 | 0.097368 | 0.073684 | 0.057895 | 0.052632 | 0.036842 | 0.025 | 0.025
DUT 6 | 1 | 0.73684 | 0.63158 | 0.52632 | 0.5 | 0.45789 | 0.38421 | 0.38421
DUT 7 | 1 | 0.038462 | 0.034231 | 0.028846 | 0.027308 | 0.023846 | 0.016538 | 0.016538

## Slide 16: TID results – idle current
Chart: Samsung, 4 Gbit, room temperature

## Slide 17: Summary
SEE results
No SEL (LET=60, normal incidence)
Software conditioning may reduce SEFI sensitivity
≈10% hard SEUs
Significant hard SEU annealing
TID results
D ≥ 150 krad: Band error pattern – triggered by page activation?
D = 300 krad: error density < 10-6
Strong temperature dependence
Significant annealing
Slight idle current increase
Future work
Band error pattern – further examination
Tests at higher temperature – 50°C? 80°C? Realistic requirement?
SEL at 60° incidence
Detailed current measurement (SEFI/SEL)

## Slide 18: Overview
Part 1: DDR3 SDRAM (M. Herrmann)
Part 2: NAND flash (K. Grürmann)
  Cross sections
    Static random SEU
    Transient SEFI
    Persistent SEFI
    Destructive failure
  Annealing
    Soft SEUs
    Hard SEUs
  MBUs

## Slide 19: NAND-Flash Static Random SEU cross section
Stuck bits from previous runs subtracted from the error count
Low LET: several orders of magnitude between 25 nm and 50 nm generation
Threshold LET substantially lower than the lowest LET of RADEF cocktail
SEU results differ at low LET from the results presented by F. Irom, JPL

## Slide 20: NAND-Flash Class B Transient SEFI cross section
Sum of row, column and block errors
Dominated by row errors
All row errors are transient

## Slide 21: NAND-Flash Class C Persistent SEFI cross section
Sum of row, column and block errors
Dominated by column errors
All column errors are persistent
One out of 2000 xenon ions generates a Class C Persistent SEFI

## Slide 22: NAND-Flash Destructive Failure (DF) cross section
Statistical nature as SEU and SEFI events
Erase or write operation no longer functional
Persistent rise (factor 4) of supply current during write operation
1 DF in 250 years in mass memory of 1000 devices @ 1 AU, GCR, Samsung 8-Gbit

## Slide 23: NAND-Flash Annealing of Soft SEUs
Two effects: a) loss of the negative floating gate charge, irreversible
b) positive charge trapping near the floating gate, reversible with time, annealing

## Slide 24: NAND-Flash Annealing with decreasing feature size
With feature size scaling, charge loss dominates over charge trapping
Trapped charge domain is restricted more and more to lower LET
Remarkably same parts with different lot codes differ substantially

## Slide 25: NAND-Flash Annealing of Hard SEUs
Steady increase of hard SEUs percentage with LET
Significant annealing of soft SEUs only at nitrogen
In contrast to the soft SEUs, typically more than one half of the hard SEUs anneal within 20 days

## Slide 26: NAND-Flash Annealing of Hard SEUs
Short term / long term Hard Error annealing
“Reverse annealing” process during first 20 minutes at xenon

## Slide 27: NAND-Flash Annealing of Hard SEUs
Increase of the hard SEU count after repeated erase-write-read cycles

## Slide 28: NAND-Flash Percentage of MBUs
In most cases corruption of the same bit in the same byte of adjacent rows
Multi bit errors (MBU) in the same byte are rare
Increase of the share of adjacent row SEUs with LET

## Slide 29: NAND-Flash MBU consisting of Soft SEU and Hard SEU
MBUs at normal incidence, Xe, LET=60
Hard SEU in the center of the MBU

## Slide 30: Summary
Addressed NAND-Flash topics
SEU
SEFI
Destructive failure
Annealing of soft and hard SEU
MBU at normal incidence

## Slide 31: References
Recent publications
  M. Herrmann et al., “Heavy ion SEE test of 2 Gbit DDR3 SDRAM”, RADECS Data Workshop, DW-28, 2011
  K. Grürmann et al., “Heavy Ion sensitivity of 16/32-Gbit NAND-Flash and 4-Gbit DDR3 SDRAM”, IEEE NSREC Data Workshop, W-9, 2012
  M. Herrmann et al., “New SEE Test Results for 4 Gbit DDR3 SDRAM”, RADECS Data Workshop, DW-25L, 2012
  K. Grürmann et al., “New SEE Test Results of 16/32-Gbit SLC NAND-Flash”, RADECS Data Workshop, DW-23L, 2012
  S. Gerardin et al., “Radiation Effects in Flash Memories”, accepted for IEEE TNS Special Issue, 2013
  M. Herrmann at al., In-Situ TID Test of 4-Gbit DDR3 SDRAM Devices, submitted to NSREC Data Workshop, 2013
DDR3 SDRAM technical notes
  M. Herrmann et al., “TID Test of 4 Gbit DDR3 SDRAM Devices”, TN-IDA-RAD-13/4
  M. Herrmann et al., “Heavy Ion SEE Test of 4 Gbit DDR3 SDRAM Devices”, TN-IDA-RAD-13/1
  M. Herrmann et al., “Unbiased TID Test of 2-Gbit and 4-Gbit DDR3 SDRAM Devices”, TN-IDA-RAD-13/9
NAND Flash technical notes
  K. Grürmann et al., “Heavy Ion SEE Test of 2-Gbit DDR3 SDRAM Devices and of 8-Gbit NAND-Flash Memory Devices, RADEF Jyväskylä, May 23 – 27, 2011”, Test Report, TN-IDA-RAD-11/5B
  K. Grürmann et al., “Heavy Ion SEE Test of 16-Gbit/32-Gbit Micron SLC NAND-Flash Memory Devices, RADEF Jyväskylä, Jan. 9 – 13, 2012, RADEF Jyväskylä, April 16 – 20, 2012”, Test Report, TN-IDA-RAD-12/12
  K. Grürmann et al., “Heavy Ion SEE Test of 4 x 8-Gbit Samsung and 16-Gbit Micron SLC NAND-Flash Memory Devices, TAMU Texas, December 4 – 7, 2012”, Test Report, TN-IDA-RAD-13/2B