Page 1 of 22

INTEGRATED CIRCUITS, SILICON MONOLITHIC,

CMOS, 128K X 8-BIT, ASYNCHRONOUS STATIC

RANDOM ACCESS MEMORY WITH THREE STATE OUTPUTS

BASED ON TYPE 6509E

ESCC Detail Specification No. 9301/053

| Issue 1 | November 2013 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2013, All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without prior permission of the European Space Agency and provided it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |

TABLE OF CONTENTS

1	General	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants	5

1.5	MAXIMUM RATINGS	5

1.6	HANDLING PRECAUTIONS	6

1.7	PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION	7

1.8	FUNCTIONAL DIAGRAM	8

1.9	PIN ASSIGNMENT	8

1.10	TRUTH TABLE AND TIMING DIAGRAMS	10

1.11	PROTECTION NETWORKS	14

2	REQUIREMENTS	14

2.1	GENERAL	14

2.1.1	Deviations from the Generic Specification	14

2.1.1.1	Deviations from Screening Tests - Chart F3	14

2.2	MARKING	14

2.3	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	15

2.3.1	Room Temperature Electrical Measurements	15

2.3.2	High and Low Temperatures Electrical Measurements	20

2.4	PARAMETER DRIFT VALUES	20

2.5	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	21

2.6	POWER BURN-IN CONDITIONS	22

2.7	1.7 OPERATING LIFE CONDITIONS	22

2.8	TOTAL DOSE RADIATION TESTING	22

2.8.1	Bias Conditions and Total Dose Level for Total Dose Radiation Testing	22

2.8.2	Electrical Measurements for Total Dose Radiation Testing	23

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 9000

MIL-STD-883, Test Methods and Procedures for Semiconductor Devices

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 930105301R

Detail Specification Reference: 9301053

Component Type Variant Number: 01

Total Dose Radiation Level Letter: R (as required)

### Component Type Variants

The component type variants applicable to this specification are as follows:

| Variant Number | Based on Type | Case | Lead Material and Finish | Weight max g | Total Dose Radiation Level Letter |
| --- | --- | --- | --- | --- | --- |
| 01 | 65609E | MFP-F32 | G2 | 3 | R [100kRAD(Si)] |

The terminal material and finish shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

The total dose radiation level letter shall be as defined in ESCC Basic Specification No 22900. If an alternative radiation test level is specified in the Purchase Order the letter shall be changed accordingly.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Supply Voltage | VDD | -0.5 to 5 | V | Note 1 |
| Input Voltage Range | VIN | -0.3 to VDD +0.3 | V | Notes 1, 2 |
| Output Voltage Range | VOUT | -0.3 to VDD +0.3 | V | Notes 1, 2 |
| Input Current | IIN | ±10 | mAdc |  |
| Output Current into Input/Outputs (Low) | II/O | 20 | mAdc | Note 3 |
| Device Power Dissipation (Continuous) | PD | 200 | mW |  |
| Operating Temperature Range | Top | -55 to +125 | oC | Tamb |
| Storage Temperature Range | Tstg | -65 to +150 | oC |  |
| Soldering Temperature | Tsol | +300 | oC | Note 4 |
| Junction Temperature | Tj | +175 | oC |  |
| Thermal Resistance Junction to Case | Rth(j-c) | 14 | oC/W |  |

NOTES:

All voltages are with respect to VSS. Device is functional from 3 ≤ VDD ≤ 3.6V

VDD + 0.3V shall not exceed 5V.

The maximum output current of any single I/O.

Duration 10 seconds maximum at a distance of not less than 1.6mm from the device body and the same terminal shall not be resoldered until 3 minutes have elapsed.

## HANDLING PRECAUTIONS

These devices are susceptible to damage by electrostatic discharge. Therefore, suitable precautions shall be employed for protection during all phases of manufacturing, testing, packaging, shipment and any handling.

These components are categorised as Class 1 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 500 Volts.

## PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION

Flat Leaded Multilayer Flat Package (MFP-F32) - 32 lead

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 1.78 | 2.72 |  |
| b | 0.38 | 0.48 | 2 |
| c | 0.076 | 0.15 | 2 |
| D | 20.62 | 21.03 | 3 |
| E | 10.26 | 10.57 | 3 |
| E2 | 6.96 | 7.26 |  |
| e | 1.27 BSC |  | 2, 4 |
| L | 7 | 8.5 | 4 |
| Q | 0.51 | 0.76 | 2, 5 |
| S | - | 1.14 | 6 |
| S1 | 0 | - | 6 |

NOTES:

Index mark: a notch or terminal 1 identification mark shall be located adjacent to terminal 1.

All terminals.

This dimension allows for package edge anomalies caused by material protrusions such as rough ceramic, misaligned ceramic layers and lids, meniscus, and glass overrun.

- The corner shape (square, notch, radius etc.) may vary at the manufacturer option from that shown on the drawing.

30 places. The true position pin spacing is 1.27mm between centrelines. Each pin centreline shall be located within ±0.13mm of its true longitudinal position relative to Pin 1 and the highest pin number.

Dimension Q shall be measured at the point of exit of the lead from the body.

Two places.

## FUNCTIONAL DIAGRAM

## PIN ASSIGNMENT

| Pin | Function |
| --- | --- |
| 1 | VDD |
| 2 | A4 Input (Address) |
| 3 | I/O2 Input/Output (Data) |
| 4 | A7 Input (Address) |
| 5 | I/O1 Input/Output (Data) |
| 6 | A3 Input (Address) |
| 7 | A6 Input (Address) |
| 8 | A8 Input (Address) |
| 9 | A0 Input (Address) |
| 10 | A1 Input (Address) |
| 11 | CS2 Input (Chip Select) |
| 12 | I/O5 Input/Output (Data) |
| 13 | A2 Input (Address) |
| 14 | Input (Write Enable) |
| 15 | I/O6 Input/Output (Data) |
| 16 | Not Connected |
| 17 | Input (Chip Select) |
| 18 | VSS |
| 19 | I/O7 Input/Output (Data) |
| 20 | Input (Output Enable) |
| 21 | A11 Input (Address) |
| 22 | I/O8 Input/Output (Data) |
| 23 | A10 Input (Address) |
| 24 | A9 Input (Address) |
| 25 | A14 Input (Address) |
| 26 | A13 Input (Address) |
| 27 | I/O4 Input/Output (Data) |
| 28 | A12 Input (Address) |
| 29 | A15 Input (Address) |
| 30 | I/O3 Input/Output (Data) |
| 31 | A16 Input (Address) |
| 32 | A5 Input (Address) |

## TRUTH TABLE AND TIMING DIAGRAMS

Logic Level Definitions: L = Low Level, H = High Level, X = Irrelevant, Z = High Impedance

| Inputs |  |  |  | Input/Outputs | Mode |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | I/On |  |
| H | X | X | X | Z | Deselect/Power down |
| X | L | X | X | Z | Deselect/Power down |
| L | H | H | L | Data out | Read |
| L | H | L | X | Data in | Write |
| L | H | H | H | Z | Output disable |

Data Retention

Write Cycle 1:  CONTROLLED HIGH during Write

Write Cycle 2: CONTROLLED LOW

Write Cycle 3: OR CONTROLLED.

Read Cycle 1: Address Controlled = = VIL, = W = VIH

Read Cycle 2: Controlled W = = VIH

Read Cycle 3: Controlled = VIL, = VIH

## PROTECTION NETWORKS

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Screening Tests - Chart F3

High Temperature Reverse Bias Burn-in shall not be performed.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component shall be:

Terminal identification.

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb=+22 ±3oC.

| Characteristics | Symbols | MIL-STD-883 Test Method | Test Conditions Note 1 | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Functional Test 1 | - | 3014 | Verify Truth Table Note 2 | - | - | - |
| Functional Test 2 | - | 3014 | Verify Truth Table Note 2 | - | - | - |
| Functional Test 3 | - | 3014 | Verify Truth Table Note 2 | - | - | - |
| Functional Test 4 | - | 3014 | Verify Truth Table Note 2 | - | - | - |
| Input Clamp Voltage, to VSS | VIC | 3008 | IIN(Under Test)= -100A All Other Pins Open VDD=Open,VSS=0V | -2 | 0.2 | V |
| Low Level Input Current | IIL | 3009 | VIN(Under Test)=0V VIN(Remaining Inputs)=3.6V VDD=3.6V, VSS=0V | - | -1 | A |
| High Level Input Current | IIH | 3010 | VIN(Under Test)=3.6V, VIN(Remaining Inputs)=0V VDD=3.6V, VSS=0V | - | 1 | A |
| Output Leakage Current, Third State, Low Level Applied 1 | IOZL1 | 3020 | VIN()=3.3V VIN(CS2)=0V VOUT=0V VDD=3.6V, VSS=0V | - | -1 | A |
| Output Leakage Current, Third State, Low Level Applied 2 | IOZL2 | 3020 | VIN()=0V VIN(CS2)=3.3V VOUT=0V VDD=3.6V, VSS=0V | - | -1 | A |
| Output Leakage Current, Third State, High Level Applied 1 | IOZH1 | 3020 | VIN()=3.3V VIN(CS2)=0V VOUT=0V VDD=3.6V, VSS=0V | - | 1 | A |
| Output Leakage Current Third State, High Level Applied 2 | IOZH2 | 3020 | VIN()=0V VIN(CS2)=3.3V VOUT=0V VDD=3.6V, VSS=0V | - | 1 | A |
| Low Level Output Voltage | VOL | 3007 | VIL=0.8V,VIH=2.2V IOL=1mA VDD=3V, VSS=0V Note 3 | - | 0.4 | V |
| High Level Output Voltage | VOH | 3006 | VIL=0.8V, VIH=2.2V IOH=-0.5mA, VDD=3V, VSS=0V Note 4 | 2.4 | - | V |
| Stand-by Supply Current 1 | IDDSB1 | 3005 | VIN()=2.2V VIN(CS2)=0.8V f=0Hz VDD=3.6V, VSS=0V Note 5 | - | 2.5 | mA |
| Stand-by Supply Current 2 | IDDSB2 | 3005 | VIN()=3.3V VIN(CS2)=0.3 V f=0Hz VDD=3.6V, VSS=0V Note 5 | - | 1.5 | mA |
| Operating Supply Current | IDDOP | 3005 | VIN(CS2, , )=3V VIN(CS1)=0V IOUT=0mA f=25MHz VDD=3.6V, VSS=0V | - | 50 | mA |
| Data Retention Current | IDDDR | 3005 | VIN()=1.8V VIN(CS2)=0.2V VDD=2V, VSS=0V Notes 5, 6 | - | 1 | mA |
| Data Retention Test | - | - | Note 6 | - | - | - |
| Input Capacitance | CIN | 3012 | VIN=VSS=VDD=0V f=1MHz Note 10 | - | 8 | pF |
| Output Capacitance | COUT | 3012 | VIN=VSS=VDD=0V f=1MHz Note 10 | - | 8 | pF |
| Read Cycle Time | tAVAV | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 40 | - | ns |
| Address Access Time | tAVQV | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | - | 40 | ns |
| Address Valid to Low Z | tAVQX | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 3 | - | ns |
| Write Cycle Time | tAVAW | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 35 | - | ns |
| Address Set-up Time | tAVWL | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 0 | - | ns |
| Address Valid to End of Write | tAVWH | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 28 | - | ns |
| Data Set-up Time | tDVWH | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | 28 | - | ns |
| Chip Select 1 Low to Write End | tE1LWH | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 28 | - | ns |
| Chip Select 2 High to Write End | tE2HWH | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 28 | - | ns |
| Write Low to High Z | tWLQZ | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | - | 15 | ns |
| Write Pulse Width | tWLWH | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | 28 | - | ns |
| Address Hold from to End of Write | tWHAX | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | 3 | - | ns |
| Data Hold Time | tWHDX | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | 0 | - | ns |
| Write High to Low Z | tWHQX | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | 0 | - | ns |
| Chip Select 1 Access Time | tE1LQV | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | - | 40 | ns |
| Chip Select 1 Low to Low Z | tE1LQX | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | 3 | - | ns |
| Chip Select 1 High to High Z | tE1HQZ | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | - | 15 | ns |
| Chip Select 2 Access Time | tE2HQV | 3003 | VDD=3 & 3.6V VSS=0V Note 8 | - | 40 | ns |
| Chip Select 2 High to Low Z | tE2HQX | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | 3 | - | ns |
| Chip Select 2 Low to High Z | tE2LQZ | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | - | 15 | ns |
| Output Enable Access Time | tGLQV | 3003 | VDD=3 & 3.6V VSS=0V Note 7 | - | 12 | ns |
| Output Enable Low to Low Z | tGLQX | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | 0 | - | ns |
| Output Enable High to High Z | tGHQZ | 3003 | VDD=3 & 3.6V VSS=0V Note 9 | - | 10 | ns |

Notes

Unless otherwise specified all inputs and outputs shall be tested for each characteristic, inputs not under test shall be VIN = VSS or VDD and outputs not under test shall be open.

Functional go-no-go test with the following test sequences:

FUNCTIONAL TEST 1

| Pattern | Timing (ns) Note (a) | VDD (V) | VSS (V) | VIL (V) | VIH (V) | IOL (mA) | IOH (mA) | Vout comp (V) Note (c) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| March | 100 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Checkerboard | 100 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Imag | 100 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Genbl | 100 | 3 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |

FUNCTIONAL TEST 2

| Pattern | Timing (ns) Note (a) | VDD (V) | VSS (V) | VIL (mV) | VIH (V) | IOL (mA) | IOH (mA) | Vout comp (V) Note (c) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| March | 100 | 3.6 | 0 | -300 | 3.9 | 0.5 | -0.5 | 1.5 |
| March | 100 | 3 | 0 | -300 | 3.3 | 0.5 | -0.5 | 1.5 |
| March | 100 | 3.6 | 0 | 0 | 2.2 | 0.5 | -0.5 | 1.5 |
| March | 100 | 3 | 0 | 800 | 0 | 0.5 | -0.5 | 1.5 |

FUNCTIONAL TEST 3

| Pattern | Timing (ns) Note (a) | VDD (V) | VSS (V) | VIL (V) | VIH (V) | IOL (mA) | IOH (mA) | Vout comp (V) Note (c) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| March | 100 | 3 | 0 | 0 | 3 | 1 | -0.5 | Note (b) |

FUNCTIONAL TEST 4

| Pattern | Timing (ns) Note (a) | VDD (V) | VSS (V) | VIL (V) | VIH (V) | IOL (mA) | IOH (mA) | Vout comp (V) Note (c) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| March | 80 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Comarch | 80 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Imag | 80 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |
| Checkerboard | 80 | 3 & 3.6 | 0 | 0 | 3 | 0.5 | -0.5 | 1.5 |

          - A write cycle is followed by a read cycle. The time between start of write and start of read per the truth table is the specified timing parameter. tr = tf ≤ 5ns.

0.4V for low output level, 2.4V for high output level.

Output load 1 TTL gate equivalent +CL<30pF.

            - Address inputs shall be selected to produce a low level at the pin under test.

Address inputs shall be selected to produce a high level at the pin under test.

Measurements are performed with the memory loaded with a background of zeros, then with a background of ones, for all inputs High, then Low. Only the worst case is recorded.

Data retention procedure:

          - Write memory at VDD = 3V with CHECKBOARD pattern with VIL = 0V and VIH = 3V.

          - Power down to VDD = 2V for 250ms, VIN()=1.8V

          - Restore VDD to 3V, wait tR(operation recovery time), read memory and compare with original pattern.

          - Repeat the procedure with pattern.

          - tR = 40ns.

          - During power up and power down transitions, VIN() ≥ VDD-0.2V, VIN(Remaining Inputs) ≤ 0.2V or ≥  VDD-0.2V.

Parameter tested go-no-go during Functional Test 4.

Parameter measured during Functional Test 4 using pattern March at 3V and 3.6V.

Guaranteed with output loading 5pF but not tested.

Guaranteed but not tested.

### High and Low Temperatures Electrical Measurements

The measurements shall be performed at Tamb=+125(+0-5)oC and Tamb=-55(+5-0)oC. The characteristics, test methods, conditions and limits shall be the same as specified for Room Temperature Electrical Measurements.

## PARAMETER DRIFT VALUES

Unless otherwise specified, the measurements shall be performed at Tamb=+22 ±3oC.

The test methods and test conditions shall be as per the corresponding test defined in Room Temperature Electrical Measurements.

The drift values (Δ) shall not be exceeded for each characteristic specified. The corresponding absolute limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value | Absolute |  |  |
|  |  |  | Min | Max |  |
| Low Level Input Current | IIL | ±0.1 | - | -1 | µA |
| High Level Input Current | IIH | ±0.1 | - | 1 | µA |
| Output Leakage Current, Third State, Low Level Applied 1 | IOZL1 | ±0.1 | - | -1 | µA |
| Output Leakage Current, Third State, Low Level Applied 2 | IOZL2 | ±0.1 | - | -1 | µA |
| Output Leakage Current, Third State, High Level Applied 1 | IOZH1 | ±0.1 | - | 1 | µA |
| Output Leakage Current, Third State, High Level Applied 2 | IOZH2 | ±0.1 | - | 1 | µA |
| Low Level Output Voltage | VOL | ±100 | - | 400 | mV |
| High Level Output Voltage | VOH | ±0.1 | 2.4 | - | V |
| Stand-by Supply Current 1 | IDDSB1 | ±0.25 | - | 2.5 | mA |
| Stand-by Supply Current 2 | IDDSB2 | ±0.15 | - | 1.5 | mA |
| Data Retention Current | IDDDR | ±0.1 | - | 1 | mA |

NOTES:

Unless otherwise specified all inputs and outputs shall be tested for each characteristic.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb=+22 ±3oC.

The characteristics, test methods, conditions and limits shall be as specified for Room Temperature Electrical Measurements.

## POWER BURN-IN CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +125 (+0 -5) | oC |
| Inputs A0 to A16 | VIN | S3 to S19 (Note 1) | V |
| Input CS1 | VIN | VSS | V |
| Input CS2 | VIN | VDD | V |
| Inputs W | VIN | VGEN(S1) (Note 2) | V |
| Input OE | VIN | VGEN(S2) (Note 2) | V |
| Inputs/Outputs I/O2, I/O4, I/O6, I/O8 | VIN | VGEN(S20) (Note 1) | V |
| Inputs/Outputs I/O1, I/O3, I/O5, I/O7 | VIN | VGEN(S21) (Note 1) | V |
| Pulse Voltage | VGEN | 0V to VDD | V |
| Pulse Frequency | fGENS3 | 330 ±20% (Note 1) | kHz |
| Positive Supply Voltage | VDD | 3.7 (±0.1) | V |
| Negative Supply Voltage | VSS | 0 | V |

NOTES:

Input waveforms to indicate required timing and phase relationship:

Input Protection Resistor = Output Load = 1 kΩ

## 1.7	OPERATING LIFE CONDITIONS

The conditions shall be as specified for Power Burn-in.

## TOTAL DOSE RADIATION TESTING

### Bias Conditions and Total Dose Level for Total Dose Radiation Testing

Continuous bias shall be applied during radiation testing as specified below.

The total dose level applied shall be as specified in the component type variant information herein or in the Purchase Order.

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Inputs An, CS2, , | VIN | VDD | V |
| Input/Outputs I/On | VIN | Open | V |
| Input | VIN | VSS | V |
| Positive Supply Voltage | VDD | 3.6 ±0.1 | V |
| Negative Supply Voltage | VSS | 0 | V |

NOTES:

Input protection resistor = 1kΩ.

### Electrical Measurements for Total Dose Radiation Testing

Prior to, during and on completion of radiation testing the devices shall successfully meet Room Temperature Electrical Measurements specified herein.

Unless otherwise specified the measurements shall be performed at Tamb = 22±3oC.

The characteristics, test methods, conditions and limits shall be the same as specified for Room Temperature Electrical Measurements.