ECSS Secretariat

ESA-ESTEC

Requirements & Standards Division

Noordwijk, The Netherlands

Space product assurance

Materials, processes and their data selection

Foreword

This Standard is one of the series of ECSS Standards intended to be applied together for the management, engineering, product assurance and sustainability in space projects and applications. ECSS is a cooperative effort of the European Space Agency, national space agencies and European industry associations for the purpose of developing and maintaining common standards. Requirements in this Standard are defined in terms of what shall be accomplished, rather than in terms of how to organize and perform the necessary work. This allows existing organizational structures and methods to be applied where they are effective, and for the structures and methods to evolve as necessary without rewriting the standards.

This Standard has been prepared by the ECSS Executive Secretariat reviewed and approved by the ECSS Technical Authority.

Disclaimer

ECSS does not provide any warranty whatsoever, whether expressed, implied, or statutory, including, but not limited to, any warranty of merchantability or fitness for a particular purpose or any warranty that the contents of the item are error-free. In no respect shall ECSS incur any liability for any damages, including, but not limited to, direct, indirect, special, or consequential damages arising out of, resulting from, or in any way connected to the use of this Standard, whether or not based upon warranty, business agreement, tort, or otherwise; whether or not injury was sustained by persons or property or otherwise; and whether or not loss was sustained from, or arose out of, the results of, the item, or any services that may be provided by ECSS.

Published by: 	ESA Requirements and Standards Division

ESTEC, P.O. Box 299,

2200 AG Noordwijk

The Netherlands

Copyright: 	2019© by the European Space Agency for the members of ECSS

Change log

| ECSS-Q-70-71A 27 February 2004 | First issue |
| --- | --- |
| ECSS-Q-70-71A Rev.1 18 June 2004 | First issue Revision 1 |
| ECSS-Q-ST-70-71B | Never issued |
| ECSS-Q-ST-70-71C 15 October 2014 | Second issue The main changes between ECSS-Q-70-71A Rev.1 and the current version are: - Change of title of standard - Redrafting of ECSS-Q-70-71A Rev.1 according to new ECSS drafting rules and template - Transfer of several requirements to ECSS-Q-ST-70C Rev.1 - Alignment of the three Standards ECSS-E-ST-32-08C Rev.1, ECSS-Q-ST-70C Rev.1 and ECSS-Q-ST-70-71C |
| ECSS-Q-ST-70-71C Rev.1 15 October 2019 | Second issue Revision 1 Major changes with respect to ECSS-Q-ST-70-71C (15 October 2014) are: - Update of the Standard due to the impact of the European Regulation "Registration, Evaluation, Authorisation and Restriction of Chemicals (REACH)" leading update of Annex A containing information about the European Space Materials Database (ESMDB). - Former informative Annex A “Information about the European Space materials database (ESMDB) deleted and information about added in clause 4.1. Detailed changes: Added requirements: - none Modified requirements: - 4.3.9.3b NOTE 4 modified Deleted requirements: - none |

Table of contents

Change log	3

1 Scope	6

2 Normative references	7

3 Terms, definitions and abbreviated terms	9

3.1	Terms from other standards	9

3.2	Terms specific to the present standard	9

3.3	Abbreviated terms	10

3.4	Nomenclature	11

4 Specific requirements	12

4.1	Overview	12

4.2	Material requirements	12

4.2.1	General requirements	12

4.2.2	Aluminium and aluminium alloys	13

4.2.3	Copper and copper alloys	13

4.2.4	Nickel and nickel alloys	14

4.2.5	Titanium and Titanium alloys	14

4.2.6	Steels	15

4.2.7	Stainless steels	15

4.2.8	Filler metals: welding, brazing, soldering	16

4.2.9	Miscellaneous metallic materials	17

4.2.10	Optical materials	18

4.2.11	Adhesives, coatings, varnishes	19

4.2.12	Adhesive tapes	20

4.2.13	Paints and inks	22

4.2.14	Lubricants	22

4.2.15	Potting compounds, sealants, foams	23

4.2.16	Reinforced plastics including PCBs	24

4.2.17	Rubbers and elastomers	25

4.2.18	Thermoplastics	26

4.2.19	Thermoset plastics or PCBs	28

4.2.20	Material aspects of wires and cables	29

4.2.21	Ceramics and other non­metallic materials	30

4.3	Process requirements	30

4.3.1	Adhesive bonding	30

4.3.2	Composite manufacture	31

4.3.3	Encapsulation and moulding and varnishing	32

4.3.4	Painting and coating	32

4.3.5	Cleaning	33

4.3.6	Welding and brazing	33

4.3.7	Crimping and stripping and wire wrapping	35

4.3.8	Soldering	36

4.3.9	Surface treatments	36

4.3.10	Plating	39

4.3.11	Machining	39

4.3.12	Forming	40

4.3.13	Heat treatment	43

4.3.14	Marking	43

4.3.15	Miscellaneous processes	44

4.3.16	Inspection procedures	46

Annex A <<deleted>>	48

Bibliography	49

# Scope

This Standard specifies the requirements applicable to materials, processes and their data selection to satisfy the mission performance requirements.

This Standard covers the following:

selection criteria and rules;

utilization criteria and rules.

The provisions of this Standard apply to all actors involved at all levels in the production of space systems. These can include manned and unmanned spacecraft, launchers, satellites, payloads, experiments, electrical ground support equipment, mechanical ground support equipment, and their corresponding organizations.

This standard may be tailored for the specific characteristics and constraints of a space project in conformance with ECSS-S-ST-00.

# Normative references

The following normative documents contain provisions which, through reference in this text, constitute provisions of this ECSS Standard. For dated references, subsequent amendments to, or revisions of any of these publications do not apply. However, parties to agreements based on this ECSS Standard are encouraged to investigate the possibility of applying the most recent editions of the normative documents indicated below. For undated references the latest edition of the publication referred to applies.

| ECSS-S-ST-00-01 | ECSS system - Glossary of terms |
| --- | --- |
| ECSS-E-ST-20-06 | Space engineering - Spacecraft charging |
| ECSS-E-ST-32-08 | Space engineering - Materials |
| ECSS-Q-ST-20 | Space product assurance - Quality assurance |
| ECSS-Q-ST-70 | Space product assurance - Materials, mechanical parts and processes |
| ECSS-Q-ST-70-02 | Space product assurance - Thermal vacuum outgassing test for the screening of space materials |
| ECSS-Q-ST-70-04 | Space product assurance - Thermal testing for the evaluation of space materials, processes, mechanical parts and assemblies |
| ECSS-Q-ST-70-07 | Space product assurance - Verification and approval of automatic machine wave soldering |
| ECSS-Q-ST-70-08 | Space product assurance - Manual soldering of high-reliability electrical connections |
| ECSS-Q-ST-70-10 | Space product assurance - Qualification of printed circuit boards |
| ECSS-Q-ST-70-11 | Space product assurance - Procurement of printed circuit boards |
| ECSS-Q-ST-70-12 | Space product assurance - Design rules for printed circuit boards |
| ECSS-Q-ST-70-18 | Space product assurance - Preparation, assembly and mounting of RF coaxial cables |
| ECSS-Q-ST-70-26 | Space product assurance - Crimping of high-reliability electrical connections |
| ECSS-Q-ST-70-28 | Space product assurance - Repair and modification of printed circuits board assemblies for space use |
| ECSS-Q-ST-70-30 | Space product assurance - Wire wrapping of high-reliability electrical connections |
| ECSS-Q-ST-70-31 | Space product assurance - Application of paints on flight hardware |
| ECSS-Q-ST-70-38 | Space product assurance - High-reliability soldering for surface-mount and mixed technology |
| ECSS-Q-ST-70-39 | Space product assurance - Processing and quality assurance requirements for welding of metallic materials for flight hardware |
| ESCC 3901 | Generic specification - Wires and cables, electrical, 600V, low frequency |
| ESCC 3902 | Generic specification - Cables, coaxial, radio frequency, flexible |
| ESCC 3903 | Generic specification - Solid wires, electrical 350 V, for wire wrapping |

# Terms, definitions and abbreviated terms

## Terms from other standards

For the purpose of this Standard, the terms and definitions from ECSS-S-ST-00-01 apply, in particular for the following terms:

assembly

component

corrosion

lot

material

part

process

relifing

repair

For the purpose of this Standard, the terms and definitions from ECSS-E-ST-32 apply, in particular for the following terms:

A-basis design allowable (A-value)

B-basis design allowable (B-value)

## Terms specific to the present standard

plate

form of material having a thickness of >6 mm

sheet

form of material having a thickness >0,2 mm and <6 mm

foil

form of material having a thickness <0,2 mm

thick coatings

coating with such a thickness that the properties of the substrate do not significantly influence the coating properties

NOTE	A thick homogeneous coating can be as such treated as if it were effectively a bulk material. The thickness is generally above approximately 125 µm.

debubbling

removal of bubbles performed by low pressure process between the coating line and the coating stand

The pressure can be high enough not to cause boiling. The low-pressure causes the bubbles to expand and thus rise faster.

unstabilized stainless steel

steels from the 300 series which do not contain Titanium or Niobium as a stabilizing element against the formation of iron-carbides

The iron-carbide formation is also called sensitization and occurs during prolonged heating at temperatures above 370 °C. Iron-carbide formation can also be avoided using lower carbon grades.

exfoliation

corrosion that proceeds along planes parallel to the surface, generally at grain boundaries, forming corrosion products that create a wedging stress, giving rise to a layered appearance

This form of corrosion is associated with a marked directionality of the grain structure. Applied stresses are not necessary for exfoliation to occur. However, in alloys susceptible to stress corrosion cracking, the corrosion product wedging action undoubtedly contributes to the propagation of the exfoliation attack. It is important to note that some alloys not susceptible to stress corrosion cracking can suffer exfoliation corrosion. However, if the grain structure is equiaxed, exfoliation corrosion does not usually occur.

## Abbreviated terms

For the purpose of this Standard, the abbreviated terms from ECSS-S-ST-00-01 and the following apply:

| Abbreviation | Meaning |
| --- | --- |
| ATOX | atomic oxygen |
| EDM | electro discharge machining |
| ESMDB | European Space Materials Database |
| DPL | declared parts list |
| GOX | gaseous oxygen |
| KIc | fracture toughness |
| KIscc | stress-corrosion cracking threshold stress intensity factor |
| LOX | liquid oxygen |
| MMPDS | metallic materials properties development and standardization |
| MPCB | materials and processes control board |
| NDI | non-destructive inspection |
| PTFE | polytetrafluroethylene |
| SCC | stress-corrosion cracking |
| UTS | ultimate tensile strength |

## Nomenclature

The following nomenclature applies throughout this document:

- The word “shall” is used in this Standard to express requirements. All the requirements are expressed with the word “shall”.

- The word “should” is used in this Standard to express recommendations. All the recommendations are expressed with the word “should”.

It is expected that, during tailoring, recommendations in this document are either converted into requirements or tailored out.

The words “may” and “need not” are used in this Standard to express positive and negative permissions, respectively. All the positive permissions are expressed with the word “may”. All the negative permissions are expressed with the words “need not”.

The word “can” is used in this Standard to express capabilities or possibilities, and therefore, if not accompanied by one of the previous words, it implies descriptive text.

In ECSS “may” and “can” have completely different meanings: “may” is normative (permission), and “can” is descriptive.

The present and past tenses are used in this Standard to express statements of fact, and therefore they imply descriptive text.

# Specific requirements

## Overview

This Standard applies together with the ECSS-Q-ST-70.

The European Space Materials Database (ESMDB) will provide free distribution knowledge in the field of Materials technologies via a shared database. A dedicated Steering Board has been created for development and the regular update of the ESMDB. This board is in charge for selection and validation process of candidate materials and relevant tools. Material property data obtained from tests by material producers, government agencies, and members of the aerospace industry are submitted to ESMDB Steering board for review and analysis. Database access will be controlled by the ESMDB Steering Board.

Hazardous chemical substances in materials, processes or in the end-product can be affected by the REACH regulation imposing actions for legal compliance or the risk of obsolescence.

Guidelines for obsolescence management for materials, mechanical parts and processes are provided in ECSS-Q-HB-70-23.

## Material requirements

### General requirements

ECSS-Q-ST-70-71_1260001

Design stresses shall include all residual stresses including those coming from manufacturing and assembly processes.

ECSS-Q-ST-70-71_1260002

Alloys, heat treatments and coatings which minimize susceptibility to general corrosion, pitting, intergranular and stress corrosion cracking shall be used.

### Aluminium and aluminium alloys

ECSS-Q-ST-70-71_1260003

Wrought heat-treatable products shall be mechanically stress relieved.

For example in TX5X or TX5XX tempers.

ECSS-Q-ST-70-71_1260004

Wrought alloys 5456, 5083 and 5086 shall be used only in controlled tempers for resistance to SCC and exfoliation.

Examples of controlled tempers are H111, H112, H116, H117, H323, H343.

ECSS-Q-ST-70-71_1260005

Long-term manned structures, shall not use aluminium alloys 2024-T6, 7079-T6 and 7178-T6 in structural applications.

ECSS-Q-ST-70-71_1260006

Black anodising shall not be used on 2000 and 7000 series of Aluminium Alloys.

The black anodizing of metals is covered by ECSS-Q-ST-70-03.

ECSS-Q-ST-70-71_1260007

Long-term manned structures, shall not use aluminium alloys 5083-H32, 5083-H38, 5086-H34, 5086-H38, 5456-H32 and 5456-H38 in applications where the temperature exceeds 66 °C.

### Copper and copper alloys

ECSS-Q-ST-70-71_1260008

For electronic assemblies applications and wirings, materials and processes shall conform to the requirements from clause 5 to clause 15 of ECSS-Q-ST-70-08 and from clause 5 to clause 16 of ECSS-Q-ST-70-38.

ECSS-Q-ST-70-71_1260009

Copper coatings shall not be used on external surfaces exposed to atomic oxygen in the low Earth orbit.

### Nickel and nickel alloys

ECSS-Q-ST-70-71_1260010

The effect of alloying element depletion at the surface of superalloys in high-temperature oxidizing environments shall be evaluated when sheet is used.

A slight amount of depletion can involve a considerable proportion of the effective cross section of the material.

ECSS-Q-ST-70-71_1260011

Any foreign material which can contain sulphur, shall be removed prior to heat treatment or high temperature service.

1	Nickel and high nickel content alloys are susceptible to sulphur embrittlement.

2	Sulphur can be contained for example in oils, grease, and cutting lubricants as well as in air.

### Titanium and Titanium alloys

ECSS-Q-ST-70-71_1260012

Hydrogen, Oxygen and Nitrogen uptake shall be avoided in all phases of the parts manufacturing or use.

1	The uptake of hydrogen during processes (with possible generation of hydrides) can occur for example on processes such as welding, cleaning and heat treatment.

2	The uptake of oxygen during processes (with possible generation of alpha cases) can occur for example during heat treatment, welding and Electro Discharge Machining.

ECSS-Q-ST-70-71_1260013

Titanium alloys whose hardenability is limited by section size shall not be used in dimensions which exceed their limits.

ECSS-Q-ST-70-71_1260014

Structural applications using titanium shall be designed to avoid fretting.

ECSS-Q-ST-70-71_1260015

For manned structures, titanium shall not be used with LOX or GOX at a pressure exceeding 34,5 kPa.

ECSS-Q-ST-70-71_1260016

For manned structures, titanium shall not be used with air where the oxygen partial pressure exceeds 34,5 kPa.

ECSS-Q-ST-70-71_1260017

The use of cleaning fluids and other chemicals that are detrimental to the performance of titanium or titanium alloy parts shall not come in contact with these metals.

### Steels

ECSS-Q-ST-70-71_1260018

All high-strength heat treated parts which are acid cleaned, plated or exposed to other hydrogen-producing processes shall be subjected to a baking process.

High-strength heat treated parts are > 1225 MPa UTS.

ECSS-Q-ST-70-71_1260019

Tempers of precipitation hardening steels that are susceptible to stress corrosion and hydrogen embrittlement shall not be used.

ECSS-Q-ST-70-71_1260020

Designs using precipitation hardening steels shall ensure the following:

controlled processing procedures are used, and

processing and procurement records are maintained for the reference.

### Stainless steels

ECSS-Q-ST-70-71_1260021

Unstabilized austenitic steels shall not be used at temperatures above 370 °C.

ECSS-Q-ST-70-71_1260022

When using 400-series stainless steels the risk for hydrogen embrittlement, corrosion and stress corrosion cracking shall be controlled.

ECSS-Q-ST-70-71_1260023

Control means shall be presented for customer approval.

### Filler metals: welding, brazing, soldering

ECSS-Q-ST-70-71_1260024

The selection of alloys to be welded and the selection of process techniques shall be in conformance with national or international aerospace specifications and standards approved by the customer.

ECSS-Q-ST-70-71_1260025

The fusion zone and the unmelted heat affected zone of a weld shall be accessible for inspection.

ECSS-Q-ST-70-71_1260026

All welds used for structural applications shall undergo 100 % radiographic inspection in conformance with specifications approved by the customer.

ECSS-Q-ST-70-71_1260027

All welds used for structural applications shall undergo a NDI program that shall be submitted for customer approval.

ECSS-E-ST-32-01 contains additional requirements specific to welds used for Potential Fracture Critical Items applications.

ECSS-Q-ST-70-71_1260028

The capability of the equipment to meet the specified requirements, processes, welding supplies and supplementary treatments selected by the supplier shall be demonstrated through qualification testing of welded specimens representing the materials and joint configuration of production parts.

ECSS-Q-ST-70-71_1260029

The selection of brazing alloys and brazing techniques shall be in conformance with national or international aerospace specifications and standards approved by the customer.

ECSS-Q-ST-70-71_1260030

Design shall include the effect of the brazing process on the strength of the parent metal.

Base metal is the example of the parent metal.

ECSS-Q-ST-70-71_1260031

Subsequent fusion welding in the vicinity of brazed or soldered joints or other operations with high temperatures that affect the brazed or soldered joint shall not be performed.

ECSS-Q-ST-70-71_1260032

Soldered joints shall not be used for structural applications.

ECSS-Q-ST-70-71_1260033

Solders, process materials and procedures for electrical and electronic assembly shall conform to the requirements from clause 5 to clause 15 of ECSS-Q-ST-70-08 and from clause 5 to clause 16 of ECSS-Q-ST-70-38.

### Miscellaneous metallic materials

ECSS-Q-ST-70-71_1260034

The supplier shall demonstrate that the selected Magnesium alloys are protected against corrosion effects with respect to the applicable environment.

ECSS-Q-ST-70-71_1260035

Hazards related to Magnesium alloys flammability during manufacturing shall be prevented.

ECSS-Q-ST-70-71_1260036

The supplier shall demonstrate that the selected Magnesium alloys are used in applications where risks of ignition are prevented.

Examples of risk areas are those subjected to wear, abuse, foreign object damage, abrasion, erosion or at any location where fluid or moisture entrapment is possible.

ECSS-Q-ST-70-71_1260037

Alloys containing Beryllium higher than 4 % by weight shall not be used.

ECSS-Q-ST-70-71_1260038

The design of parts made of beryllium alloys shall include the material’s low impact resistance, notch sensitivity, its anisotropy and sensitivity to surface finish requirements.

ECSS-Q-ST-70-71_1260039

The application of refractory alloys shall be subjected to approval by the customer.

Limited amount of data for structural assessment are available on these materials.

ECSS-Q-ST-70-71_1260040

Silver and Osmium coatings shall not be used on external surfaces of space systems exposed to atomic oxygen in low Earth orbit.

ECSS-Q-ST-70-71_1260041

Platings with open porosity shall be sealed.

ECSS-Q-ST-70-71_1260042

The selection of a superalloy for a given application shall be based on tests of the material in simulated in-service environments.

ECSS-Q-ST-70-71_1260043

Foreign material which contains sulphur shall be removed from superalloys prior to heat treatment or high-temperature service.

Examples of materials that can contain sulphur are: oils, grease and cutting lubricants.

ECSS-Q-ST-70-71_1260044

The effect of alloying element depletion in superalloys at the surface in a high-temperature oxidizing environment shall be evaluated when sheet is used.

### Optical materials

ECSS-Q-ST-70-71_1260045

The supplier shall demonstrate that the performances of the selected optical glasses or coatings are not degraded below the specified acceptable levels by ionizing radiation, particle, UV radiation and ATOX for the intended application.

ECSS-Q-ST-70-71_1260046

Use of glasses for the structural applications shall be in conformance with requirements 4.2.21a, 4.2.21b and 4.2.21c.

ECSS-Q-ST-70-71_1260047

When organic glasses are used, a radiation resistance assessment shall be performed.

ECSS-Q-ST-70-71_1260048

In assemblies incorporating optical materials, it shall be demonstrated that the difference in thermal expansion coefficients between the optical material and its mounting within the specified range of temperatures does not prevent to meet the design requirements.

### Adhesives, coatings, varnishes

ECSS-Q-ST-70-71_1260049

The surfaces on which the adhesives, coatings or varnishes are applied shall be clean and dry prior to their application.

ECSS-Q-ST-70-71_1260050

Structural adhesive bonds in honeycomb panels shall attach the facings rigidly to the core to allow loads to be transmitted from one face to another.

ECSS-Q-ST-70-71_1260051

Adhesives, coatings and varnishes shall be physically and chemically compatible with the component parts of the finished assembly.

This includes for example the adherends for adhesives, substrates and any other parts, such as materials used in the insulation or bodies of electronic components for coatings.

ECSS-Q-ST-70-71_1260052

Adhesives, coatings and varnishes shall be capable of accommodating dimensional changes resulting from temperature excursions without causing damage to the adhesive bond, or to other parts of the assembly.

Electronic PCBs are example of other parts of the assembly.

ECSS-Q-ST-70-71_1260053

The supplier shall demonstrate that the mismatch of thermal expansion coefficients between adherends and adhesive or between substrates and coatings is within the design requirements.

ECSS-Q-ST-70-71_1260054

When acceptability of the mismatch of thermal expansion coefficients between adherends and adhesive is verified by test, the test procedure shall conform to the requirements of clause 5 of ECSS-Q-ST-70-04.

ECSS-Q-ST-70-71_1260055

When acceptability of the mismatch of thermal expansion coefficients between substrates and coatings is verified by test, the test procedure shall conform to the requirements of clause 5 of ECSS-Q-ST-70-04.

ECSS-Q-ST-70-71_1260056

Applications of thick coatings that can result in damage to the coated items shall be evaluated by testing.

Resulting damage can be for example: high residual stresses, high temperatures during cure.

ECSS-Q-ST-70-71_1260057

Alkyd-, polyester- or polysulphide-type coatings shall not be used.

ECSS-Q-ST-70-71_1260058

Any compound that contains or releases corrosive media that can attack adjacent parts of the assembly shall be assessed for its potential risk.

Examples of corrosive media are: acetic acid, ammonia, amines, hydrochloric and other acids.

ECSS-Q-ST-70-71_1260059

The supplier shall verify that the curing is affecting the whole surface of the bonded area when adhesives need atmospheric moisture as part of the curing process.

This verification is even more important in case of non-porous or large surfaces.

ECSS-Q-ST-70-71_1260060

The supplier shall demonstrate that solvents contained in coatings and varnishes have been removed prior to curing.

Thinner is example of solvent.

ECSS-Q-ST-70-71_1260061

Adhesives, coatings and varnishes that are sensitive to moisture contamination shall only be used in controlled-humidity environments.

ECSS-Q-ST-70-71_1260062

Where void free application is used on coatings and varnishes the supplier shall apply a debubbling process, defined in a dedicated procedure.

### Adhesive tapes

ECSS-Q-ST-70-71_1260063

Tapes containing polyvinylchloride shall not be used in space segment elements or ground segment equipment undergoing vacuum.

ECSS-Q-ST-70-71_1260064

All release agents present on the surface of tapes shall be removed.

ECSS-Q-ST-70-71_1260065

The adherent surface or surfaces on which the tape is applied shall be clean and dry prior to its application.

ECSS-Q-ST-70-71_1260066

When an adhesive tape is applied to painted surfaces, the supplier shall verify that the paint is not degraded when the adhesive tape is removed.

ECSS-Q-ST-70-71_1260067

An even pressure shall be used on the tape during its application.

ECSS-Q-ST-70-71_1260068

It shall be ensured that the tape is not damaged during its application.

ECSS-Q-ST-70-71_1260244

Perforated tapes should be used to enable the correct evacuation of trapped air bubbles underneath the adhesive tape.

ECSS-Q-ST-70-71_1260069

When perforated tapes are not used, the process of tape application and removal of bubbles shall be documented.

ECSS-Q-ST-70-71_1260070

The exposure to the space environment shall not impair the function of the tape.

ECSS-Q-ST-70-71_1260071

Surfaces that have had tapes removed for reworking or for temporary reasons shall be cleaned after the tape is removed.

Adhesives, in particular silicone ones, can leave a residue which prevents adhesion of other systems onto that surface.

ECSS-Q-ST-70-71_1260072

Removed tapes shall not be reused.

ECSS-Q-ST-70-71_1260073

The supplier shall demonstrate that the selected Velcro-type tape does not release hooks or felt during assembly or disassembly.

ECSS-Q-ST-70-71_1260074

Conductive adhesive tapes shall be tested to ensure that the specified conductivity and adhesion are maintained at temperature extremes.

### Paints and inks

ECSS-Q-ST-70-71_1260075

The surfaces on which paints or inks are applied shall be clean and dry prior to their application.

ECSS-Q-ST-70-71_1260076

Contamination of painted surfaces shall be prevented.

For non-moisture curing paints, environmental control applies.

ECSS-Q-ST-70-71_1260077

Painted surfaces shall be protected from mechanical damage.

Examples of mechanical damage: scratches and chips.

ECSS-Q-ST-70-71_1260078

Electrical properties of paints shall comply with the requirements from the clause 6 of ECSS-E-ST-20-06.

The requirements to be compliant with, are relevant to external surface materials, where charging requirements apply.

### Lubricants

ECSS-Q-ST-70-71_1260079

The selection of the lubricant shall avoid the contamination of the lubricated part.

ECSS-Q-ST-70-71_1260080

Lubricants shall only be applied to clean surfaces.

ECSS-Q-ST-70-71_1260081

Lubricated items shall be protected from contamination.

Examples of contamination are: dust and dirt.

ECSS-Q-ST-70-71_1260082

When oils and greases are directly exposed to space environment, the supplier shall demonstrate that the selected grade complies with the mission requirements.

ECSS-Q-ST-70-71_1260083

Graphite alone shall not be used as lubricant under vacuum.

Under vacuum conditions graphite is not a lubricant but an abrasive. It can be used in combination with other lubricating materials such as silver or MoS2.

ECSS-Q-ST-70-71_1260084

The long-term performance of lubricants shall be assessed during their selection for long-term deployed systems.

ECSS-Q-ST-70-71_1260085

Lubricants containing chloro-fluoro compositions shall not be used with aluminium or magnesium if shear stresses are imposed.

### Potting compounds, sealants, foams

ECSS-Q-ST-70-71_1260086

Polysulphide potting material shall not be used.

ECSS-Q-ST-70-71_1260087

Non-metallic foams with an open-cell structure shall not be used.

Open-cell foams are difficult to keep clean.

ECSS-Q-ST-70-71_1260088

The supplier shall assess the effect of shrinkage or the production of exothermic temperatures during curing before use.

ECSS-Q-ST-70-71_1260089

Surface treatments shall be used in conformance with process procedures approved by the customer on components and assemblies to ensure adhesion between the component and the potting compound or sealant.

Examples of surface treatments: etching and priming.

ECSS-Q-ST-70-71_1260090

The supplier shall assess the need of using pre-coating to ensure proper adhesion between the part and the potting compound or sealant and reduce residual stresses created during curing.

ECSS-Q-ST-70-71_1260091

Where void free potting application is used, the supplier shall apply a debubbling process, defined in a dedicated procedure.

ECSS-Q-ST-70-71_1260092

Foams with fully closed-cell structure shall not be debubbled.

ECSS-Q-ST-70-71_1260093

All filler materials used in potting compounds shall be dry, as defined by the supplier in a dedicated specification.

ECSS-Q-ST-70-71_1260094

The supplier shall demonstrate that the cure procedures are performed such that the temperatures and pressures created during curing process do not damage the potting compound or the parts being potted.

ECSS-Q-ST-70-71_1260095

All potting, coating and sealing materials used successively shall be evaluated for compatibility.

Some chemical or atmospheric constituents can affect those of another material.

ECSS-Q-ST-70-71_1260096

Catalysts and hardeners shall be evaluated for their compatibility with any metals present in the assembly.

### Reinforced plastics including PCBs

ECSS-Q-ST-70-71_1260097

The design and verification of fibre-reinforced composite materials used for structural applications shall conform to the requirements from clause 4 of ECSS-E-ST-32-08.

ECSS-Q-ST-70-71_1260098

Composite materials made with polyester containing styrene shall not be used.

ECSS-Q-ST-70-71_1260099

The individual stages of all processing of reinforced plastics shall be controlled and monitored in conformance with approved quality control and inspection procedures.

These can include, for example, correct lay-up of plies, no or low void content, absence of defects, absence of contamination, results of test coupons and non-destructive evaluation.

ECSS-Q-ST-70-71_1260100

Natural reinforcing materials shall not be used for electronic composite laminates.

1	Cotton and paper are examples of natural reinforcing materials.

2	PCBs are example of electronic composite laminates.

ECSS-Q-ST-70-71_1260101

Qualification of electronic PCBs shall conform to the requirements from clause 5 to clause 9 of ECSS-Q-ST-70-10.

ECSS-Q-ST-70-71_1260102

Procurement of electronic PCBs shall be in conformance with requirements from clause 5 to clause 7 of ECSS-Q-ST-70-11.

### Rubbers and elastomers

ECSS-Q-ST-70-71_1260103

Designs using rubber and elastomeric materials shall be assessed for:

“set” under stress,

effects of cyclic stress,

environmental resistance, and

chemical resistance.

ECSS-Q-ST-70-71_1260104

Polysulphide materials shall not be used in the space environment.

ECSS-Q-ST-70-71_1260105

Chlorinated materials shall not be used in space environments.

ECSS-Q-ST-70-71_1260106

Silicone materials shall not be used in pressurized systems requiring low gas permeability.

ECSS-Q-ST-70-71_1260107

Rubbers and elastomers containing plasticisers or extending oils shall not be used under vacuum.

ECSS-Q-ST-70-71_1260108

The leaching of filler materials shall be assessed with respect to their potential hazard to associated equipment.

ECSS-Q-ST-70-71_1260109

Material depolymerization due to vacuum exposure shall be assessed.

ECSS-Q-ST-70-71_1260110

Rubbers or elastomers releasing corrosive media shall be assessed for its potential risk.

ECSS-Q-ST-70-71_1260111

Materials that liberate acetic acid shall be assessed before use.

ECSS-Q-ST-70-71_1260112

Rubbers and elastomers used in long-term, manned structures shall be assessed for their long-term resistance to the following:

ageing,

low temperature,

ozone,

heat-ageing,

polymer reversion,

working fluids,

lubricants and operating media and,

any application- or mission-specific requirements.

ECSS-Q-ST-70-71_1260113

The cure date of rubbers and elastomers shall be recorded.

ECSS-Q-ST-70-71_1260245

The cured date of rubbers and elastomers should be indicated on the part.

ECSS-Q-ST-70-71_1260114

For rubbers and elastomers, environmental exposure shall be assessed.

Examples of environmental exposure are: flammability requirements, electrical requirements, normal use temperature, abnormal use temperature excursions, chemical exposure and humidity levels.

### Thermoplastics

ECSS-Q-ST-70-71_1260115

Structural designs using thermoplastic composite materials shall conform to the requirements of clause 4 of ECSS-E-ST-32-08.

ECSS-Q-ST-70-71_1260116

For polymer-based materials, a definition of all the design constraints shall be established.

1	Examples of polymer-based materials are thermosetting and thermoplastic.

2	Examples of design constraints are: short-term loading, long-term loading, cyclic loading, impact loading, design life and critical dimensional tolerances.

ECSS-Q-ST-70-71_1260117

Thermoplastics shall be evaluated for the effects of service conditions.

ECSS-Q-ST-70-71_1260118

A structural design analysis shall be performed on all parts incorporating polymer-based materials, including the visco-elastic nature of the chosen material.

ECSS-Q-ST-70-71_1260119

For polymer-based materials prototypes shall be produced and tested to qualify the design.

Examples of polymer-based materials are thermosetting and thermoplastic.

ECSS-Q-ST-70-71_1260120

For polymer-based materials, environmental exposure shall be assessed.

Examples of environmental exposure are: flammability requirements, electrical requirements, normal use temperature, abnormal use temperature excursions, chemical exposure and humidity levels.

ECSS-Q-ST-70-71_1260121

The supplier shall demonstrate that the anisotropic characteristics of plastic films are assessed during design.

ECSS-Q-ST-70-71_1260122

The supplier shall demonstrate how the processing methods of thermoplastics accounts for their softening temperature.

ECSS-Q-ST-70-71_1260123

PTFE shall not be used in creep resistance applications.

ECSS-Q-ST-70-71_1260124

Thermoplastics that retain residual stresses after processing shall be subject to an approved thermal stress-relief process.

ECSS-Q-ST-70-71_1260125

The release of additives in plastics under vacuum shall be assessed for their effect on the material performance and contamination risk.

ECSS-Q-ST-70-71_1260126

Materials that absorb and release water shall be assessed with respect to the effect on the performance of the material and for contamination risk.

ECSS-Q-ST-70-71_1260127

Cellulose and acetate materials in the form of films shall not be used in space applications.

ECSS-Q-ST-70-71_1260128

Polyamide films shall be assessed for moisture-related effects.

ECSS-Q-ST-70-71_1260129

Polyvinyl acetate shall not be used in space applications.

ECSS-Q-ST-70-71_1260130

Polyvinyl butyrate shall not be used in space applications.

ECSS-Q-ST-70-71_1260131

Multi-layer systems shall be vented to eliminate internal overpressure.

ECSS-Q-ST-70-71_1260132

Multi-layer systems shall be baked to an approved process prior to integration into the space segment elements.

### Thermoset plastics or PCBs

ECSS-Q-ST-70-71_1260133

Structural design of components using thermosetting resins shall conform to the requirements of clause 4 of ECSS-E-ST-32-08.

Examples of thermoset plastics are fibre reinforced composites.

ECSS-Q-ST-70-71_1260134

Thermosetting plastics shall be assessed for the effects of service conditions.

ECSS-Q-ST-70-71_1260135

Curing processes shall be assessed by means of a preliminary test programme using thermal-analysis equipment.

ECSS-Q-ST-70-71_1260136

Resins used in PCBs for space hardware shall be qualified in conformance with requirements from clause 5 to clause 9 of ECSS-Q-ST-70-10.

ECSS-Q-ST-70-71_1260137

Polyester resins shall not be used for space applications.

### Material aspects of wires and cables

ECSS-Q-ST-70-71_1260138

General requirements for wires and cables shall be in conformance with requirements from ESCC Generic Specifications 3901, 3902 and 3903.

ECSS-Q-ST-70-71_1260139

Electrical wires and cables shall be procured in conformance with the requirements of ESCC Generic Specification 3901.

Electrical wires and cables are 600 V, low frequency.

ECSS-Q-ST-70-71_1260140

Coaxial, radiofrequency, flexible cables shall be procured in conformance with the requirements ESCC Generic specification 3902.

ECSS-Q-ST-70-71_1260141

The materials for coaxial cable assembly shall be selected in conformance with requirements from clause 5 of ECSS-Q-ST-70-18.

ECSS-Q-ST-70-71_1260142

For wires with insulating material made of PTFE or other non-treated fluorocarbons, the supplier shall demonstrate that workmanship avoids cold flow.

1	Examples of good practices are controlled bend radii, no contact with sharp objects, wire fixation rules.

2	The use of irradiated ETFE-Ethylenetetrafluroethylene (TEFZEL) wires with improved characteristics against cold flow is preferred.

### Ceramics and other non­metallic materials

ECSS-Q-ST-70-71_1260143

Ceramics and glasses, except as fibres, shall not be used in a structural applications without the prior approval of the customer.

ECSS-Q-ST-70-71_1260144

Engineering data used to justify the selection and demonstrate the strength of ceramics and glasses for structural uses shall be subject to review and approval by the customer.

ECSS-Q-ST-70-71_1260145

All applications using composite materials based on ceramic, carbon and glass compositions shall be reviewed and approved by the customer.

ECSS-Q-ST-70-71_1260146

Products containing asbestos shall not be used.

## Process requirements

### Adhesive bonding

ECSS-Q-ST-70-71_1260147

The supplier shall demonstrate the ability to reproduce the specified bonding quality.

ECSS-Q-ST-70-71_1260148

Process conditions and environments shall be specified and controlled during all stages of adhesive bonding.

Adhesive bonding stages include preparation, application, curing or drying, inspection or testing and storage.

ECSS-Q-ST-70-71_1260149

Surfaces to be bonded shall be cleaned and prepared by a surface treatment process.

Examples of treatment process are abrasion or chemical etching, release film or peel ply removed before bonding.

ECSS-Q-ST-70-71_1260150

Prepared surfaces shall be protected from contaminants.

ECSS-Q-ST-70-71_1260151

Prepared surfaces shall be stored in controlled environment within a specified maximum duration demonstrated during the verification phase.

ECSS-Q-ST-70-71_1260152

During the bonding process, the adhesive cure cycle shall be controlled in accordance with an established procedure approved by the customer.

For guidelines on structural adhesive bonding see ECSS-E-HB-32-21.

ECSS-Q-ST-70-71_1260153

The supplier shall demonstrate that the bonded primary structural joints show cohesive failure modes in shear testing.

1	Good toughness and peel strength are applicable characteristics for structural adhesives.

2	An insert system consists of a removable threaded fastener and a fixture that is embedded into the honeycomb structure using a potting compound. The general processing steps for installing inserts include:

machining the honeycomb panel, normally using specific tools

potting the insert

curing the potting material.

3	For guidelines on the use of inserts see ECSS-E-HB-32-22.

### Composite manufacture

ECSS-Q-ST-70-71_1260154

Process conditions and environments shall be specified and controlled during all stages of composite manufacture.

1	Manufacturing stages include for example: storage or de-storage and handling of raw materials, preparation, application, curing, machining, inspection or testing and storage of finished parts.

2	See ECSS-E-HB-32-20 for information on composite manufacture.

ECSS-Q-ST-70-71_1260155

Tooling materials shall be selected to ensure thermal-expansion matching between the composite over the processing temperatures.

The rigidity of the tooling is also an important parameter.

### Encapsulation and moulding and varnishing

ECSS-Q-ST-70-71_1260156

Process conditions and environments shall be specified and controlled during all stages of encapsulation, moulding and varnishing.

Stages of encapsulation moulding and varnishing include for example preparation, application, curing or drying, inspection or testing and storage.

ECSS-Q-ST-70-71_1260157

In electronic assemblies, when potting is used for encapsulation it shall allow rework or repair.

ECSS-Q-ST-70-71_1260158

In electronic assemblies conformal coating shall be used on populated boards.

### Painting and coating

ECSS-Q-ST-70-71_1260159

Processes developed for all types of paints shall be implemented and controlled in conformance with requirements from clause 4 of ECSS-Q-ST-70-31.

ECSS-Q-ST-70-71_1260160

Process conditions and environments shall be specified and controlled during all stages of painting, coating.

Stages of painting, coating include for example preparation, application, curing or drying, inspection or testing and storage.

ECSS-Q-ST-70-71_1260161

Pre-treatment processes for the surfaces to be painted shall be selected and controlled to ensure adhesion of the paint to the substrate.

Pre-treatment processes include for example cleaning, abrasion and priming.

### Cleaning

ECSS-Q-ST-70-71_1260162

Cleaning agents and processes not included in the cleaning associated procedures referenced in the DPL in conformance with DRD from the Annex C of the ECSS-Q-ST-70 shall not be used.

ECSS-Q-ST-70-71_1260163

Solvent shall not degrade the base material or that of adjacent parts.

1	For example, polymer materials adjacent to metals.

2	This requirement can imply to control not only the solvents used, but also the way they are applied.

ECSS-Q-ST-70-71_1260164

Cleaning processes shall not degrade the base material, any applied surface coating or finishes, or adjacent parts.

1	Surface coatings include for example paint and varnish.

2	Labels can also be damaged by cleaning.

3	Cleaning processes including for example submerging in solvent baths and use of ultrasonic cleaning can induce damage.

ECSS-Q-ST-70-71_1260165

Cleaning processes shall be used to remove all chemical residues produced during manufacture and assembly.

This include for example cutting oils and dye-penetrants.

### Welding and brazing

ECSS-Q-ST-70-71_1260166

All welding processes shall conform to the requirements from clause 5 to 13 of ECSS-Q-ST-70-39.

ECSS-Q-ST-70-71_1260167

Welding techniques used in aerospace engineering shall be selected as a result of an assessment of the following:

parent metals to be joined,

effect of the welding process on material properties in the fusion zone, heat affected zone and parent metal,

filler material.

In the aerospace industry the following welding techniques are used:

tungsten inert gas (TIG);

metal inert gas (MIG);

plasma-arc welding;

electron beam welding (EB);

resistance welding (induction, spot, seam);

diffusion welding;

laser welding; and

friction stir welding.

ECSS-Q-ST-70-71_1260168

The selection of alloys to be welded shall be performed in conformance with national or international aerospace specifications and standards.

ECSS-Q-ST-70-71_1260169

The selection of welding techniques shall be performed in conformance with the requirement from clause 5 to 13 of ECSS-Q-ST-70-39.

ECSS-Q-ST-70-71_1260170

The selected welding processes shall provide:

the weld quality specified in the selected standard,

the minimum weld energy input, and

protection from contamination.

ECSS-Q-ST-70-71_1260171

The capability of the equipment to meet the specified requirements, the welding process documentation including process variants, the filler material and any supplementary treatments shall be demonstrated through qualification testing of welded specimens representing the materials and the joint configuration of production parts.

ECSS-Q-ST-70-71_1260172

Each operator shall be trained and certified in accordance with the requirements from clause 6 and 7 from ECSS-Q-ST-70-39, along with the applicable welding equipment and related procedure for specific welding tasks.

ECSS-Q-ST-70-71_1260173

In long-term, manned structures, alloyed titanium shall be welded using alloy weld filler wire and not commercially pure filler wire.

ECSS-Q-ST-70-71_1260174

Welded assemblies of corrosion resistant steels shall be heat treated after welding, except for stabilized steels or low carbon grades.

ECSS-Q-ST-70-71_1260175

Equipment and procedures used for welding shall be certified for their capability to produce welds and weld repairs.

ECSS-Q-ST-70-71_1260176

The weld repair process and inspection shall be performed only under nonconformance review board approval.

ECSS-Q-ST-70-71_1260177

The weld repair process and inspection shall be qualified to the same level of assurance as the primary process specification drawing requirement using the same inspection technique that found the original defect and by all other methods of examination that were originally specified for the affected part.

ECSS-Q-ST-70-71_1260178

The result weld repair process qualification and inspection shall be subject to review by the customer.

ECSS-Q-ST-70-71_1260179

Brazing processes shall be evaluated regarding the effect on the parent metal.

ECSS-Q-ST-70-71_1260180

The supplier shall demonstrate that in case the subsequent fusion welding is applied, it is not affecting any brazed joints in the vicinity.

ECSS-Q-ST-70-71_1260181

Brazing operations shall be carried out by trained operators, working with documented and approved brazing procedures.

### Crimping and stripping and wire wrapping

ECSS-Q-ST-70-71_1260182

Fabrication processes and controls used in crimping of electrical terminations, terminal lugs, splices and two-piece shield termination rings shall conform to the requirements from clause 5 of ECSS-Q-ST-70-26.

ECSS-Q-ST-70-71_1260183

Fabrication processes and controls used in wire wrapped electrical connections shall conform to the requirements from the clause 5 of ECSS-Q-ST-70-30.

### Soldering

ECSS-Q-ST-70-71_1260184

Soldered joints shall not be used for structural applications without the prior approval of the customer.

ECSS-Q-ST-70-71_1260185

Fabrication processes and controls used in soldering of electrical connections shall conform to the requirements from clause 5 of ECSS-Q-ST-70-07, from clause 5 to clause 15 of ECSS-Q-ST-70-08 and from clause 5 to clause 16 of ECSS-Q-ST-70-38.

ECSS-Q-ST-70-71_1260186

Repair processes and controls used in soldering of electrical connections shall conform to the requirements of clause 5 of ECSS-Q-ST-70-28.

ECSS-Q-ST-70-71_1260187

The supplier shall demonstrate that when subsequent fusion welding or brazing is applied, it is not affecting any soldered joints in the vicinity.

### Surface treatments

#### General

ECSS-Q-ST-70-71_1260188

All surface treatments process specifications shall include the qualified thickness range.

ECSS-Q-ST-70-71_1260189

Processes and materials shall not degrade the substrate and result in loss of performance or integrity.

ECSS-Q-ST-70-71_1260190

The supplier shall demonstrate that the surface is free from defects and it is not stained or discoloured.

ECSS-Q-ST-70-71_1260191

An assessment shall be performed to demonstrate that the CTE mismatches between coating and substrates, if exist, do not prevent to meet the specified requirements.

1	Surfaces of materials are often treated for the following reasons:

To improve properties, e.g. nitriding, carburising and shot-peening.

To increase resistance to an environment, e.g. corrosion, moisture- and diffusion barriers, high-temperature and ATOX.

To provide particular characteristics, e.g. thermo-optical properties.

2	Some surface treatments are also included in other processes, for example preparation prior to painting and adhesive bonding to improve adhesion. These can include a proprietary “chemical” process such as anodizing or alodining or the application of a primer.

#### Anodizing

ECSS-Q-ST-70-71_1260192

The supplier shall demonstrate that when anodizing processes are applied to thin foils, the perforation is prevented.

ECSS-Q-ST-70-71_1260193

The supplier shall demonstrate that when anodizing processes are applied to thin foils the complete removal of process chemicals in complex parts is ensured.

Thin foils include for example honeycomb cores.

ECSS-Q-ST-70-71_1260194

Anodized layers shall be sealed and be continuous when used as the final surface finish of a part.

ECSS-Q-ST-70-71_1260195

Anodized surfaces for pre-treatment of painting shall not be sealed.

ECSS-Q-ST-70-71_1260196

Process conditions shall be implemented and controlled.

1	Process conditions include for example bath constituents, temperature and time.

2	Anodizing is an electrolytic process for thickening and stabilizing the inherent oxide films on metal substrates. Anodizing is widely used on aluminium alloys and can be applied to magnesium and titanium. The anodized layer is electrically non-conductive.

3	Not all grades of an alloy can be anodized successfully.

4	Depending on the precise process, anodizing can produce:

hard anodized wear resistant and durable surfaces;

coloured surfaces (either functional or decorative), e.g. black for optical properties;

pre-treatment process prior to adhesive bonding or painting.

5	Specifications for aerospace anodizing processes are available (often of American origin), but bath constituents and process conditions tend to vary between organizations.

#### Chemical conversion

ECSS-Q-ST-70-71_1260197

Chemical conversion layers shall be continuous when used as the final surface finish of a part.

ECSS-Q-ST-70-71_1260198

Control of process conditions shall be implemented and controlled.

1	Process conditions include for example bath constituents, temperature and time.

2	Chemical conversion processes involve the absorption of a protective metal oxide film into an existing oxide film. The resulting surface finish can be electrically conductive or non-conductive.

3	Non-metal oxide films may sometimes be used.

4	Chemical conversion processes include:

Chromating (mixed metal-chromium oxide film), providing good corrosion resistance and pre-treatment for subsequently applied organic coatings.

Conversion coatings for the replacement of hexavalent chromium are emerging, e.g. trivalent chromium systems.

Phosphating, used as a pre-treatment prior to painting on ferrous materials.

### Plating

ECSS-Q-ST-70-71_1260199

Process conditions and environments shall be specified and controlled during all stages of plating.

Plating stages include for example preparation, application, inspection or testing, and storage.

ECSS-Q-ST-70-71_1260200

Platings with open porosity shall not be used.

1	Porous platings fail to provide adequate corrosion protection and can act as sources of contamination.

2	Plated layers of less than 1 µm thickness tend to be porous.

ECSS-Q-ST-70-71_1260201

An post-plating baking process approved by the customer shall be applied to materials with known or suspected susceptibility to hydrogen embrittlement.

ECSS-Q-ST-70-71_1260202

Plating of terminals used in electronic assemblies, shall satisfy the requirements from clause 5 to clause 15 of ECSS-Q-ST-70-08.

ECSS-Q-ST-70-71_1260203

In electronic assemblies, processes used for the removal of gold plating shall satisfy the requirements from clause 7.2.3.2 of ECSS-Q-ST-70-08.

ECSS-Q-ST-70-71_1260204

All platings shall be blister tested by heat quench testing into air with a dwell time in the oven allowing to reach the maximum temperature seen in production and verification phases.

### Machining

ECSS-Q-ST-70-71_1260205

Machining shall not be performed on martensitic steel hardened to ≥1225 MPa UTS.

1	Machining include for example drilling or grinding.

2	Numerous different machining operations are used for aerospace materials. International or national aerospace standards and specifications are normally applied.

3	Special tools and processes are applied to the machining of composites (laminates and honeycomb panels) to prevent damage to the materials (e.g. delamination, break-out on the backface and distortion of the core) that degrade the material integrity.

4	For guidelines on machining composites, see ECSS-E-HB-32-20.

ECSS-Q-ST-70-71_1260206

When machining is performed, the formation of untempered martensite shall be prevented.

Formation of untempered martensite can be prevented e.g. by the use of carbide tipped tooling.

ECSS-Q-ST-70-71_1260207

The consequences of the effects of the use of EDM machining processes shall be assessed and reflected in any machining specification.

The use of EDM machining processes may lead to the formation of re-cast layer on the materials surfaces that has detrimental effects on the fatigue performances.

ECSS-Q-ST-70-71_1260208

Safety equipment in accordance with the specified process shall be provided for operators processing beryllium and beryllium-copper alloys.

ECSS-Q-ST-70-71_1260209

The collection and disposal of dust and debris produced during the processing of beryllium and beryllium-copper alloys shall conform to national or international specifications approved by the customer.

### Forming

#### Overview

Although forming processes are applied to metallic-, polymer-based and ceramic-type materials, this applies only to metal forming. Metal forming processes generally form two main groups:

“Warm” or “hot”: rolling, forming, various forging techniques.

“Cold”:

primary forming by various sheet metal techniques, e.g. deep drawing and bending, or

finishing operations, e.g. cold forging and cold rolling.

Specialized techniques used in the manufacture of certain spacecraft parts include:

superplastic forming, e.g. panel sections and tanks;

“gatorising”: forging with superplastic materials, e.g. integral turbine blades or discs;

explosive forming, e.g. tanks and sections.

Process selection is influenced by the material to be formed, its specific composition and mechanical properties plus the requirements of the finished formed part, e.g. shape, size, strength and appearance.

#### Forging

ECSS-Q-ST-70-71_1260210

Forging techniques shall be used that produce an internal grain-flow pattern such that the direction of flow is parallel to principal stresses.

ECSS-Q-ST-70-71_1260211

Evaluation of flow patterns, including test data shall be submitted as part of the approval procedure for forged components.

The mechanical properties are optimum in the direction of material flow during forging.

#### Sheet metal forming

ECSS-Q-ST-70-71_1260212

Forming processes shall respect the minimum bend radii for the specific alloy and condition.

Example of condition is heat-treatment or temper.

ECSS-Q-ST-70-71_1260213

Annealing processes shall be selected to avoid degradation of the material.

ECSS-Q-ST-70-71_1260214

Hot forming temperatures and soak times shall be selected to avoid segregation effects at grain boundaries or liquation of low melting point alloy constituents, either during heating the material or as a result of localized “over-heating” during forming.

1	All forming processes for sheet metals involve plastic deformation of the material. Processing techniques are either conducted “cold”, or “warm or hot”.

2	The amount of deformation possible without fracture is linked to the material ductility.

ECSS-Q-ST-70-71_1260215

For materials which harden as a result of cold working normally, an annealing process shall be applied to achieve the final shape without cracking or fracture.

1	High-strength materials are difficult to form to complex shapes by cold forming, and can be done “warm or hot”.

2	Forming is often followed by a final heat-treatment to restore the mechanical properties of the finished part.

#### Superplastic forming

ECSS-Q-ST-70-71_1260216

Superplastic forming processes shall only be applied to materials meeting the following conditions:

microstructure: 1 µm to 5 µm grain size and stable at process temperature,

plastic deformation in the range of 100 % to 1500 %, without fracture,

heated to at least 50 % of the melting temperature (in K),

relatively low forming stresses,

low deformation rate.

1	Materials meeting these conditions are said to behave superplastically.

2	Commercial superplastic alloys include those based on aluminium, titanium, copper, nickel, stainless- and carbonsteels.

3	Depending on the metal alloy, super plastic forming can be combined with diffusion bonding to create finished parts, such as struts, cylinders and integrally stiffened panels.

4	See ECSS-E-HB-32-20 for superplastic forming processes.

#### Explosive forming

ECSS-Q-ST-70-71_1260217

Safety procedures shall be applied for the storage and handling of explosives.

1	Explosive forming is a rapid process for producing small quantities of large, fairly simply-shaped parts. It is applied to materials retaining acceptable ductility at high plastic deformation rates.

2	Explosive forming is also used as a cladding process and for joining dissimilar metals that cannot be joined effectively by any other means.

### Heat treatment

ECSS-Q-ST-70-71_1260218

Heat treatment of metals and alloys shall conform to national or international specifications for aerospace applications approved by the customer.

ECSS-Q-ST-70-71_1260219

Heat treatment procedures that are not included in any national or international specifications shall be approved by the customer prior to their use.

ECSS-Q-ST-70-71_1260220

Processes shall be selected and controlled to avoid the dezincification of brasses.

### Marking

ECSS-Q-ST-70-71_1260221

Marking of spacecraft piece parts for identification purposes shall not result in the degradation of any mechanical or surface characteristics.

ECSS-Q-ST-70-71_1260222

Solvents in inks shall not attack substrates.

ECSS-Q-ST-70-71_1260223

Inks shall have outgassing properties in conformance with the requirements from clause 5 of ECSS-Q-ST-70-02.

ECSS-Q-ST-70-71_1260224

Engraving of painted, plated or coated parts shall not be performed.

ECSS-Q-ST-70-71_1260225

Stamping resulting in stress-raisers shall not be performed.

### Miscellaneous processes

#### Overview

Bolts offer the greatest strength for mechanical fastened joints, providing that they are not over-tightened and no damage occurs during assembly. For guidelines on the design of bolted joints, see ECSS-E-HB-32-23.

Riveted joints are permanent and are normally sealed against the environment. Disassembly can only be done by drilling out the rivets. Consequently, riveted joints cannot be used where access is used, or expected, to internal or adjacent parts of the structure. For guidelines on riveted joints in composites, see ECSS-E-HB-32-20.

#### Casting

ECSS-Q-ST-70-71_1260226

Quality control and inspection procedures of all process related factors influencing the performance and integrity of castings shall be implemented and controlled to all of them.

Process-related factors influencing the performance and integrity of castings include for example gas bubbles, inclusions and porosity, shrinkage.

#### Printed circuit boards

ECSS-Q-ST-70-71_1260227

Design of printed circuit board shall conform to the requirements from clause 5 to 15 of ECSS-Q-ST-70-12.

ECSS-Q-ST-70-71_1260228

Procurement of printed circuit boards used for fabrication processes and controls shall conform to the requirements from clause 5 to clause 7 of ECSS-Q-ST-70-11.

ECSS-Q-ST-70-71_1260229

Qualification of printed circuit boards used for fabrication processes and controls shall conform to the requirements from clause 5 to 9 of ECSS-Q-ST-70-10.

#### Printed circuit assemblies

ECSS-Q-ST-70-71_1260230

Fabrication processes and controls used in staking and conformal coating of printed circuit boards and electronic assemblies shall conform to the requirements of from clause 5 to clause 15 of ECSS-Q-ST-70-08, from clause 5 of ECSS-Q-ST-70-07 and from clause 5 to clause 16 of ECSS-Q-ST-70-38.

ECSS-Q-ST-70-71_1260231

The repair and modification of printed circuit boards assemblies shall conform to the requirements from clause 4 of ECSS-Q-ST-70-28.

#### Wire and cable assemblies

ECSS-Q-ST-70-71_1260232

The processes to be used for coaxial cable assembly shall be selected in conformance with clause 5 of ECSS-Q-ST-70-18.

Silver-plated copper strands are the preferred conductors. These are suitable for soldering and crimping.

- The general requirements for wires and cables assemblies are described by the ESCC standards.

ECSS-Q-ST-70-71_1260233

If Nickel plated copper strands are used the supplier shall demonstrate that solderability after ageing is as described by the generic specification.

Nickel is magnetic and cannot be used for all applications.

ECSS-Q-ST-70-71_1260234

Tin-plated finishes electroplated other than pure tin-coated wires shall be either re-flowed or excluded.

ECSS-Q-ST-70-71_1260235

Silver-plated wires shall be procured in conformance with requirements from the ESCC Generic Specification 3901.

ECSS-Q-ST-70-71_1260236

The individual wire specification of silver-plated wires shall be applied for requirements other than the ones specified in 4.3.15.5a, b, c and d.

ECSS-Q-ST-70-71_1260237

The following shall be assembled or installed in conformance with the requirements from clause 5 to clause 15 of ECSS-Q-ST-70-08:

electrical connectors;

interconnecting cables, harness and wiring;

solder splice.

ECSS-Q-ST-70-71_1260238

Solder sleeves shall not be used in flight hardware due to their retention of solder flux and inspection difficulties.

#### Fibre optic assemblies

ECSS-Q-ST-70-71_1260239

Fabrication processes and controls shall be established for terminations, joining fibre optic cable assemblies and their installation and submitted to the customer for approval.

ECSS-Q-TM-70-51 contains guidelines referring to the assembly of fibre optic.

### Inspection procedures

ECSS-Q-ST-70-71_1260240

All NDI processes shall be selected according to aerospace national or international standards, and be submitted to the customer for customer approval.

Many different inspection procedures are employed for spacecraft materials and processes are numerous and varied. They are used at all stages of the manufacturing process and form part of the overall quality assurance plan.

ECSS-Q-ST-70-71_1260241

Inspection procedures shall contain the material, the part, the classification of defects and establish their acceptance and rejection criteria.

1	The ability to inspect a part is a critical part of the design development.

2	Some inspection procedures can be relatively straightforward, for example visual inspection by unaided eye; whereas others are complex and need equipment that is regularly maintained and calibrated to recognized, approved standards, for example eddy current and ultrasonic.

ECSS-Q-ST-70-71_1260242

Acceptance and rejection criteria shall be defined according to aerospace national or international standards approved by the customer or qualification testing.

ECSS-Q-ST-70-71_1260243

Inspection equipment shall be maintained and calibrated in conformance with the clause 5.2.6 from ECSS-Q-ST-20.

<<deleted>>

Bibliography

| ECSS-S-ST-00 | ECSS system - Description, implementation and general requirements |
| --- | --- |
| ECSS-Q-ST-70-03 | Space product assurance - Black-anodizing of metals with inorganic dyes |
| ECSS-Q-HB-70-23 | Space product assurance - Materials, mechanical parts and processes obsolescence management handbook |
| ECSS-Q-TM-70-51 | Space product assurance - Termination of optical fibres |
| ECSS-E-HB-32-20 | Space engineering - Structural materials handbook |
| ECSS-E-HB-32-21 | Space engineering - Adhesive bonding handbook |
| ECSS-E-HB-32-22 | Space engineering - Insert design handbook |
| ECSS-E-HB-32-23 | Space engineering - Threaded fasteners handbook |