ECSS Secretariat

ESA-ESTEC

Requirements & Standards Division

Noordwijk, The Netherlands

Space product assurance

Processing and quality assurance requirements for metallic powder bed fusion technologies for space applications

Foreword

This Standard is one of the series of ECSS Standards intended to be applied together for the management, engineering, product assurance and sustainability in space projects and applications. ECSS is a cooperative effort of the European Space Agency, national space agencies and European industry associations for the purpose of developing and maintaining common standards. Requirements in this Standard are defined in terms of what shall be accomplished, rather than in terms of how to organize and perform the necessary work. This allows existing organizational structures and methods to be applied where they are effective, and for the structures and methods to evolve as necessary without rewriting the standards.

This Standard has been prepared by the ECSS-Q-ST-70-80C Working Group, reviewed by the ECSS Executive Secretariat and approved by the ECSS Technical Authority.

Disclaimer

ECSS does not provide any warranty whatsoever, whether expressed, implied, or statutory, including, but not limited to, any warranty of merchantability or fitness for a particular purpose or any warranty that the contents of the item are error-free. In no respect shall ECSS incur any liability for any damages, including, but not limited to, direct, indirect, special, or consequential damages arising out of, resulting from, or in any way connected to the use of this Standard, whether or not based upon warranty, business agreement, tort, or otherwise; whether or not injury was sustained by persons or property or otherwise; and whether or not loss was sustained from, or arose out of, the results of, the item, or any services that may be provided by ECSS.

Published by: 	ESA Requirements and Standards Section

ESTEC, P.O. Box 299,

2200 AG Noordwijk

The Netherlands

Copyright: 	2021© by the European Space Agency for the members of ECSS

Change log

| ECSS-Q-ST-70-80C 30 July 2021 | First issue |
| --- | --- |

Table of contents

Change log	3

Introduction	11

1 Scope	12

2 Normative references	13

3 Terms, definitions and abbreviated terms	14

3.1	Terms from other standards	14

3.2	Terms specific to the present standard	14

3.3	Abbreviated terms	15

3.4	Nomenclature	17

4 Principles	18

4.1	General	18

5 General	20

5.1	Referential axis definition	20

5.2	Safety classification of AM parts	21

5.2.1	Overview	21

5.2.2	Definition of AM safety classes	21

5.2.3	Requirement	22

5.3	Multiple laser systems	22

5.4	Family of parts	22

5.4.1	Overview	22

5.4.2	Requirements	23

5.5	Acceptance criteria	23

6 AM definition phase	24

6.1	Overview	24

6.2	Input for AM definition phase	24

6.2.1	Overview	24

6.2.2	Requirement	24

6.3	Preliminary Manufacturing Concept Review (PMCR)	25

7 Verification phase	26

7.1	Overview	26

7.2	Establishment of pAMP	26

7.2.1	Feedstock	26

7.2.2	Establishment of work processing windows including post processing	26

7.2.3	Preliminary Additive Manufacturing Procedure (pAMP)	27

7.3	Verification on specimen- (AMP), and prototype-level (HFP)	28

7.4	Additive Manufacturing Verification Plan (AMVP)	29

7.4.1	Overview	29

7.4.2	Safety class 1.1, 1.2, and class 2	29

7.4.3	Safety class 3	30

7.4.4	Reporting	31

7.5	Prototype verification Plan (PVP)	31

7.5.1	General	31

7.5.2	Safety classes 1.1, 1.2, and 2	32

7.5.3	Safety class 3	33

7.5.4	Reporting	34

7.6	Re- verification of AM machines	34

7.6.1	Overview	34

7.6.2	Requirements	34

7.7	Machine pause	35

7.7.1	Overview	35

7.7.2	Requirements	35

7.8	Repair	35

7.9	Manufacturing supports	36

7.10	Parts cleaning	36

7.11	Documentation	36

7.12	Manufacturing Readiness Review (MRR)	36

8 Hardware production	38

8.1	Overview	38

8.2	Requirements for hardware production	38

8.2.1	General	38

8.2.2	Process interruption	38

8.2.3	Manufacture of hardware and witness samples	39

8.3	Testing of witness samples	40

8.3.1	Tensile testing	40

8.3.2	Full height blanks	40

8.3.3	Powder capture sample	41

8.4	Inspection of hardware	41

8.4.1	Non-destructive techniques	41

8.5	Reporting	43

9 AM operation and supervision personnel	44

9.1	Overview	44

9.2	AM supervisor	44

9.3	Qualification and certification of AM operators	44

9.3.1	Laser based Powder Bed Fusion processes	44

9.3.2	Electron Beam based Powder Bed Fusion processes	45

9.4	Qualification and certification of personnel for NDT	45

9.5	Safety of Personnel	45

10 Equipment and facilities	46

10.1	Overview	46

10.2	Conditions for facilities	46

10.3	Laser based equipment calibration	46

10.4	Electron beam based equipment calibration	46

10.4.1	Frequency	46

10.4.2	Calibration protocol description	47

10.5	Maintenance and repair	47

10.5.1	Maintenance of laser based machines	47

10.5.2	Maintenance of electron beam based machines	48

10.5.3	Repair	50

10.6	Materials and consumables	51

10.6.1	Management of powder	51

10.6.2	Tooling and features	51

10.6.3	Gases	52

10.6.4	Cleaning of machines	52

11 Quality assurance	53

11.1	Configuration control	53

11.2	Maintenance of AM procedure	53

11.2.1	Overview	53

11.2.2	Requirements	53

11.3	Statistical Process Control	53

11.3.1	Materials Properties Database (MPD)	53

11.4	Quality control	54

11.4.1	Reference and witness samples	54

11.4.2	Documentation of manufacturing	54

11.4.3	Anomalies and non-conformances occurring during the AM process	54

11.5	Auditing	55

11.6	End Item Data Pack	55

12 Testing of AM materials and parts	56

12.1	Overview	56

12.2	Powder capture sample	56

12.2.1	Overview	56

12.2.2	Requirement	56

12.3	NDT for AM	56

12.4	Density testing	58

12.4.1	Overview	58

12.4.2	Requirements	58

12.5	Destructive testing	59

12.5.1	Metallography	59

12.5.2	Tensile testing	61

12.5.3	Fatigue testing	62

13 Powders	63

13.1	Testing of powders	63

13.2	Procurement	64

13.3	Safe Handling	65

13.4	Storage	65

13.5	Loading	66

13.6	Recycling	66

13.7	Blending	66

13.8	Disposal	67

Annex A (normative) Preliminary Manufacturing Concept Review (PMCR) - DRD	68

A.1	DRD identification	68

A.1.1	Requirement identification and source document	68

A.1.2	Purpose and objective	68

A.2	Expected response	68

A.2.1	Scope and content	68

A.2.2	Special remarks	68

Annex B (normative) Additive Manufacturing Procedure (AMP) - DRD	69

B.1	DRD identification	69

B.1.1	Requirement identification and source document	69

B.1.2	Purpose and objective	69

B.2	Expected response	69

B.2.1	Scope and content	69

B.2.2	Additional requirements for various AM processes	70

B.2.3	Special remarks	71

Annex C (normative) AM verification plan (AMVP) - DRD	72

C.1	DRD identification	72

C.1.1	Requirement identification and source document	72

C.1.2	Purpose and objective	72

C.2	Expected response	72

C.2.1	Scope and content	72

C.2.2	Special remarks	72

Annex D (normative) AM Verification Report (AMVR) – DRD	73

D.1	DRD identification	73

D.1.1	Requirement identification and source document	73

D.1.2	Purpose and objective	73

D.2	Expected response	73

D.2.1	Scope and content	73

D.2.2	Special remarks	73

Annex E (normative) Hardware Fabrication Procedure (HFP) - DRD	74

E.1	DRD identification	74

E.1.1	Requirement identification and source document	74

E.1.2	Purpose and objective	74

E.2	Expected response	74

E.2.1	Scope and content	74

E.2.2	Special remarks	74

Annex F (normative) Hardware Production Report (HPR) - DRD	75

F.1	DRD identification	75

F.1.1	Requirement identification and source document	75

F.1.2	Purpose and objective	75

F.2	Expected response	75

F.2.1	Scope and content	75

F.2.2	Special remarks	75

Annex G (normative) Prototype Verification Plan (PVP) - DRD	76

G.1	DRD identification	76

G.1.1	Requirement identification and source document	76

G.1.2	Purpose and objective	76

G.2	Expected response	76

G.2.1	Scope and content	76

G.2.2	Special remarks	76

Annex H (normative) Prototype Verification Report (PVR) - DRD	77

H.1	DRD identification	77

H.1.1	Requirement identification and source document	77

H.1.2	Purpose and objective	77

H.2	Expected response	77

H.2.1	Scope and content	77

H.2.2	Special remarks	77

Annex I (normative) Powder Management Plan (PMP) - DRD	78

I.1	DRD identification	78

I.1.1	Requirement identification and source document	78

I.1.2	Purpose and objective	78

I.2	Expected response	78

I.2.1	Scope and content	78

I.2.2	Special remarks	78

Annex J (informative) Template for auditing	79

J.1.2	Special remarks	84

Annex K (informative) Example of a Materials Properties Database (MPD)	85

Bibliography	86

Figures

Figure 4-1: Flow chart showing the steps required to establish a verified metallic Powder Bed Fusion process and consequently to produce hardware	19

Figure 5-1 Definition of coordinate system [source: EN ISO ASTM 52921:2016]	20

Figure 12-1: Melt pool measurement concept [Image and concept: adopted from NASA MSFC-SPEC-3717]	61

Tables

Table 5-1: Safety classes	22

Table 7-1: Pre-verification test matrix	27

Table 7-2: Test methods for class 1.1, 1.2, and class 2 parts	29

Table 7-3: Test methods for prototypes, and witness samples for safety classes 1.1, 1.2, and 2	32

Table 7-4: Test methods for prototypes, and witness specimens for safety class 3	33

Table 8-1: Overview of witness samples to be produced with hardware	38

Table 8-2: Overview of non-destructive tests for AM hardware	42

Table J-1 : Audit template	79

Table K-1 : Example of a Materials Properties Database	85

Introduction

This Standard specifies the processing and quality assurance requirements for the different types of Powder Bed Fusion (PBF) Additive Manufacturing processes for Metallic Materials for space flight applications. It can also be used for Additive Manufacturing activities on space related ground equipment and development activities for flight hardware. The Standard covers all Powder Bed Additive Manufacturing processes using Laser or Electron Beam as melting source.

This standard may be tailored for the specific characteristic and constraints of a space project in conformance with ECSS-S-ST-00.

# Scope

This Standard defines requirements for processing and quality assurance of powder bed fusion technologies for space applications.

Within this standard a set of phases are specified, each to be followed when defining, verifying and manufacturing parts using metallic powder bed fusion technologies. In addition, requirements for operating and supervision personnel and equipment facilities are described.

This Standard does not aim to prescribe process parameters relevant to the fabrication using metallic powder bed fusion technologies.

Although this standard is developed for powder bed fusion based techniques, its principles can also be used as a reference for other metal-based and polymer-based processes. These include Wire Arc Additive Manufacturing (WAAM), Stereolithography (with metals), Binder Jetting, but also Selective Laser Sintering (SLS), Stereolithography (with polymers), Fused Deposition Modelling (FDM), and others.

# Normative references

The following normative documents contain provisions which, through reference in this text, constitute provisions of this ECSS Standard. For dated references, subsequent amendments to, or revision of any of these publications do not apply. However, parties to agreements based on this ECSS Standard are encouraged to investigate the possibility of applying the more recent editions of the normative documents indicated below. For undated references, the latest edition of the publication referred to applies.

| ECSS-S-ST-00-01 | ECSS system – Glossary of terms |
| --- | --- |
| ECSS-E-ST-32 | Space engineering - Structural general requirements |
| ECSS-Q-ST-10-09 | Space product assurance - Nonconformance control system |
| ECSS-Q-ST-20 | Space product assurance - Quality assurance |
| ECSS-Q-ST-70 | Space product assurance - Materials, mechanical parts and processes |
| ECSS-Q-ST-70-15 | Space product assurance - Non-destructive testing |
| ECSS-Q-ST-70-45 | Space product assurance -Mechanical testing of metallic materials |
| EN 2003-009:2007 | Aerospace series - Test methods - Titanium and titanium alloys - Part 009: Determination of surface contamination |
| EN ISO ASTM 52921:2016 | Standard terminology for additive manufacturing - Coordinate systems and test methodologies |
| ISO 2859-1:1999 | Sampling procedures for inspection by attributes, Part 1: Sampling schemes indexed by acceptance quality limit (AQL) for lot‐by‐lot inspection |
| ISO ASTM 52941:2020 | Additive manufacturing - System performance and reliability - Acceptance tests for laser metal powder-bed fusion machines for metallic materials for aerospace application |
| ISO ASTM 52942:2020 | Additive manufacturing - Qualification principles - Qualifying machine operators of laser metal powder bed fusion machines and equipment used in aerospace applications |

# Terms, definitions and abbreviated terms

## Terms from other standards

For the purpose of this Standard, the terms and definitions from ECSS-S-ST-00-01 apply.

For the purpose of this Standard, the terms and definitions from ECSS-E-ST-32 apply, in particular for the following term:

structure

## Terms specific to the present standard

as built

condition of a part or material sample that did not receive any treatment after completion of the AM build job

build job configuration

design of the part, its location, the number of the part(s) and witness specimens, in addition to supporting strategy in the build volume

build job

single complete operation of the powder bed fusion process to create objects in the powder bed

Multiple objects are commonly created during a build job.

[adopted from NASA MSFC 3717]

structural part

declaration by the design authority of an application to be structural or non-structural

The term “structural design” is defined in clause 3.2.44 of ECSS-E-ST-32 and can give some guidelines on how to declare an application structural or non-structural.

fatigue critical part

declaration by the design authority of a part to be fatigue critical or not

Typical cases are where fatigue loads are a significant factor in the design and verification process.

post process operations

action(s) performed after completion of the build job

powder lot

one quantity of powder manufactured in one continuous operation

powder batch

some quantity of a powder lot

When a large quantity of powder is procured (from the same powder lot), the powder lot is often split into different batches. Different batches can be blended, but they all originate from the same powder lot.

re-verification

repetition of a verification program or parts of it

The conditions are specified in clause 7.6.

end-to-end manufacturing process

process of producing AM parts, including any pre- and post-processing

overlap zone

part of the build volume of an AM machine, where sub-volumes of parts are built by two or more lasers or electron beams

evenly distributed in the build volume

distributed such that locations in the x-y plane, but also in z-direction up to the maximum height of the part to be built are covered

manufacturing supports

mechanical connections to limit parts distortion and to allow heat transfer during manufacturing

## Abbreviated terms

For the purpose of this Standard, the abbreviated terms and symbols from ECSS-S-ST-00-01 and the following apply:

| Abbreviation | Meaning |
| --- | --- |
| AM | additive manufacturing |
| AMP | additive manufacturing procedure |
| AMVP | additive manufacturing verification plan |
| AMVR | additive manufacturing verification report |
| AQL | acceptance quality level |
| ASTM | American Society for Testing and Materials |
| CDR | critical design review |
| CoC | certificate of compliance |
| DI | de-ionised |
| DRD | document requirements definition |
| E-PBF | Electron Beam Powder Bed Fusion |
| ECSS | European Cooperation for Space Standardization |
| EDS | energy-dispersive spectrometry |
| EIDP | end item data pack |
| ELI | extra low interstitials |
| FM | flight model |
| Ftu | ultimate tensile strength |
| Fty | yield strength |
| GSTP | general support technology program |
| HFP | hardware fabrication procedure |
| HIP | hot isostatic pressing |
| HP | hardware production |
| HPR | hardware production report |
| IPA | isopropyl alcohol |
| ISO | International Organisation for Standardisation |
| LBB | leak before burst |
| L-PBF | Laser Powder Bed Fusion |
| MMPDS | Metallic Materials Properties Development and Standardization |
| MOC | molecular contamination |
| mPBF | metal powder bed fusion |
| MPD | materials properties database |
| MRR | manufacturing readiness review |
| NCR | nonconformance report |
| NDT | non-destructive testing |
| OEM | original equipment manufacturer |
| PAC | particulate contamination |
| pAMP | preliminary additive manufacturing procedure |
| PBF | powder bed fusion |
| pHFP | preliminary hardware fabrication procedure |
| PMCR | preliminary manufacturing concept review |
| PVP | prototype verification plan |
| PVR | prototype verification report |
| RFA | request for approval |
| RFW | request for waiver |
| SEM | scanning electron microscope |
| SPC | statistical process control |
| X-Ray CT | x-ray computed tomography |

## Nomenclature

The following nomenclature applies throughout this document:

- The word “shall” is used in this Standard to express requirements. All the requirements are expressed with the word “shall”.

The word “should” is used in this Standard to express recommendations. All the recommendations are expressed with the word “should”.

It is expected that, during tailoring, recommendations in this document are either converted into requirements or tailored out.

The words “may” and “need not” are used in this Standard to express positive and negative permissions, respectively. All the positive permissions are expressed with the word “may”. All the negative permissions are expressed with the words “need not”.

The word “can” is used in this Standard to express capabilities or possibilities, and therefore, if not accompanied by one of the previous words, it implies descriptive text.

In ECSS “may” and “can” have completely different meanings: “may” is normative (permission), and “can” is descriptive.

The present and past tenses are used in this Standard to express statements of fact, and therefore they imply descriptive text.

# Principles

## General

Producing parts through metallic Powder Bed Fusion technologies occurs frequently during the manufacture of parts for space applications.

This Standard specifies the necessary requirements to perform metallic Powder Bed Fusion processes for space applications (see Figure 4-1). Firstly, it is comprised of three phases, as they typically occur during the development of additively produced space hardware:

Within the AM definition phase, hardware requirements are reviewed and compared with AM manufacturing constraints, allowing for an early assessment of the feasibility of the envisaged AM project. At this stage, it is clarified, whether or not an existing, verified AMP is applicable for the intended application. If this is the case, the verification on specimen level in point 2 is not repeated, but the verification on part level is then the next step.

The aim of the verification phase is to verify the AM end-to-end process through a dedicated test campaign on specimen and part level. The verification on specimen-level results in the approved AMP. The HFP then summarises this two-stage verification on prototype-level and constitutes the basis for any hardware production. The intent of the AMP is to describe the intrinsic material properties and can therefore also be used for other designs.

In the hardware production phase, the hardware is produced according to the HFP. The success of manufacturing and inspection is described in the HPR.

Additive Manufacturing processes are considered critical (see the definition of a critical process in ECSS-Q-ST-70) and many factors are known to have a substantial influence on the properties of the final product. Therefore, after the here above described development phases, three clauses, namely clause 9 “AM operation and supervision personnel”, 10 “Equipment and facilities”, and 11 “Quality assurance” address the suitability of operating and supervision personnel, the applied equipment and facilities and define quality assurance requirements.

Figure 4-1: Flow chart showing the steps required to establish a verified metallic Powder Bed Fusion process and consequently to produce hardware

# General

## Referential axis definition

ECSS-Q-ST-70-80_1480001

The standard axis shall be specified in accordance with EN ISO ASTM 52921:2016.

ECSS-Q-ST-70-80_1480002

The gas flow over the powder bed as well as the recoating direction shall be specified, using the referential axis definition.

ECSS-Q-ST-70-80_1480003

The Z-axis shall be perpendicular to the build platform, as specified in Figure 5-1.

ECSS-Q-ST-70-80_1480004

The X-axis shall be perpendicular to the z axis and parallel to the front side of the machine.

ECSS-Q-ST-70-80_1480005

The positive direction shall be left to right, as specified in Figure 5-1.

ECSS-Q-ST-70-80_1480006

The positive Y-axis shall be perpendicular to the Z and X-axis front to back.

ECSS-Q-ST-70-80_1480007

Figure 5-1 Definition of coordinate system [source: EN ISO ASTM 52921:2016]

## Safety classification of AM parts

### Overview

Additively manufactured parts for space applications are classified into four classes according to their function and requirements using safety categories (see clause 5.2.2).

Different considerations are made for the classification.

For example, loaded parts subjected to a maximum Von Mises stress > 50 % of the yield strength (Fty in tensile) or > 25 % of the ultimate strength (Ftu in tensile) of the material, or if in human spaceflight and subjected to fracture control, are likely considered structural in this context.

Another example is pressurized hardware designed primarily for the storage of pressurized fluid with an energy level greater than or equal to 19310 Joule, or with an internal pressure greater than or equal to 0,69 MPa, or which can create a hazard (if released) are also likely considered structural. Items with an energy level below 19310 Joule can still be considered as structural, unless for instance verified as Leak Before Burst (LBB), to mitigate the risk of catastrophic rupture (see ECSS-E-ST-32-01), although those are sometimes still considered safety critical, even if not fracture critical.

### Definition of AM safety classes

#### Safety Class 1.1 parts

Are considered critical and structural. Failure of a Class 1.1 part results in a loss of spacecraft, major components, loss of life, or loss of control of the spacecraft.

#### Safety Class 1.2 parts

Are critical, but non-structural. Failure of a Class 1.2 part results in loss of spacecraft, major components, loss of life, or loss of control of the spacecraft.

#### Safety Class 2 parts

Are non-critical but structural. Their failure can reduce the efficiency of the system but not cause the loss of the spacecraft.

#### Safety Class 3 parts

Are non-critical and non-structural and are contained so that failure does not affect other flight elements. These parts require minimal integrity verification, the controls are mainly visual.

### Requirement

ECSS-Q-ST-70-80_1480008

The customer and the design authority shall agree on a safety class for the intended product, as specified in Table 5-1.

ECSS-Q-ST-70-80_1480220

Table 5-1: Safety classes

|  | Structural | Non-structural |
| --- | --- | --- |
| Critical | Class 1.1 | Class 1.2 |
| Non-critical | Class 2 | Class 3 |

## Multiple laser systems

ECSS-Q-ST-70-80_1480009

If AM systems with multiple lasers are used, means to test the overlap zone(s) of lasers shall be implemented.

ECSS-Q-ST-70-80_1480010

If AM machines with multiple interacting lasers are used, all laser interaction areas, including the overlap zone(s) shall be assessed by testing.

The intention is to build test specimens, which are built by two lasers to assess the interface zone of these.

## Family of parts

### Overview

The intention of this clause is to allow for design modifications, of a previously verified design, which are not expected to have an impact on the manufacturing stability nor on the final properties of the part without going through a full verification.

### Requirements

ECSS-Q-ST-70-80_1480011

If design modifications are performed on parts which have previously been verified in compliance with requirement 7.5.4a, the supplier may propose to re-use the PVR of the initial design, to create a new HFP.

ECSS-Q-ST-70-80_1480012

The new HFP, specified in requirement 5.4.2a, which then does not undergo full verification, shall be submitted to the customer for approval.

## Acceptance criteria

ECSS-Q-ST-70-80_1480013

Acceptance criteria for all tests shall be specified prior to entering the prototype verification phase.

# AM definition phase

## Overview

The aim of the AM definition phase is to converge to a preliminary manufacturing concept, allowing for an early assessment of the envisaged AM project. Conducting a feasibility study before starting the AM definition phase intends to help identifying critical aspects at an early stage.

## Input for AM definition phase

### Overview

Requirements are defined in order to be able to converge to a preliminary manufacturing concept.

Requirements can refer to: mission and purpose of the part, functionality, applicable safety class, geometry of the part, interface location, thermal and mechanical loading, acceptance criteria for defects, cleanliness aspects, surface conditions, inspectability, etc.

Changes or additions of basic requirements at a later stage of the project can drastically reduce the performance of a part or in worst case require a complete redesign potentially leading to higher cost and effort in the subsequent phases. The design can be developed through co-engineering meetings between the customer, the supplier, and its major partners for post-processing.

This can include the addition of material to ease e.g. milling, which is removed before delivery, but can impact the surface finish. Areas for marking and the associated technique(s) can also be discussed during these meetings.

### Requirement

ECSS-Q-ST-70-80_1480014

AM manufacturing constraints shall be iterated with requirements, which are applicable to the part to be built, to converge to an AM end-to-end process.

1	AM manufacturing constraints can refer to: design allowables of the MPD, safety class, build volume, feature sizes (e.g. thin walled structures) maximum buildable overhang, availability of feedstock, post processing constraints (e.g. accessibility, clamping), the removal strategy for powder and manufacturing supports.

2	Cleanliness requirements which also address cleanability of the part, can significantly influence the design.

3	Violated AM design constraints in the AM definition phase can lead to a complete redesign or in worst case to abandonment of the AM concept and to higher cost and effort in the verification phase.

## Preliminary Manufacturing Concept Review (PMCR)

ECSS-Q-ST-70-80_1480015

As a result from the AM definition phase, a Preliminary Manufacturing Concept Review (PMCR) shall be performed.

ECSS-Q-ST-70-80_1480016

The minimum content of the PMCR shall be in accordance with the DRD from Annex A.

ECSS-Q-ST-70-80_1480017

If the customer declares the PMCR successful, the supplier shall proceed with further development.

# Verification phase

## Overview

The aim of this phase is to verify the AM end-to-end process through a dedicated test campaign. First, the preliminary Additive Manufacturing Procedure (pAMP) is established, defining acceptable powder characteristics, AM machine operation parameters, AM machine processing window(s), post processing parameters (e.g. pressure and working distance for jet blasting or heat treatment parameters), and NDT techniques. These parameters are then verified through rather low-cost tests (e.g. density cubes and tensile tests). Once the result of these are acceptable, the pAMP is established.

After having established the pAMP, it is verified on specimen level (AMP), and on prototype level (HFP). The main principle is that preliminary procedures (pAMP and pHFP) are converted to verified procedures (AMP and HFP) through dedicated test campaigns (AMVP and PVP). This logic is also shown in Figure 4-1.

## Establishment of pAMP

### Feedstock

ECSS-Q-ST-70-80_1480018

The powder procurement specification shall be specified in conformance with clause 13.2.

### Establishment of work processing windows including post processing

ECSS-Q-ST-70-80_1480019

The supplier shall specify a set of AM processing parameter ranges suitable for the selected alloy, design features, and supporting structure.

Examples of design features that can be foreseen are overhangs.

ECSS-Q-ST-70-80_1480020

The supplier shall specify a set of processing parameters for post-processing operations.

The post build operations are established in an early stage of the part design and printing definition as they can have an impact on its resulting features in terms of functionality, performances, appearance and safety.

ECSS-Q-ST-70-80_1480021

The supplier shall provide evidence of the general suitability of the AM and post processing parameters through testing in accordance with Table 7-1.

ECSS-Q-ST-70-80_1480022

The pre-verification phase need not be repeated for machines of the same model, for which a valid AMP exists.

ECSS-Q-ST-70-80_1480023

Table 7-1: Pre-verification test matrix

| Test definition | Quantity | Characteristics / criteria |
| --- | --- | --- |
| Tensile | At least 3 specimens each in x or y, and z direction, 9 in total | See clause 12.5.2 |
| Density | At least 3 specimens | See clause 12.4 |
| Metallography | At least 3 specimens | To be done in accordance with clause 12.5.1 with the exception of requirement 12.5.1.2 (analysis of melt pool depth) |
| Customised tests | To be specified, if requested by the customer | - |

### Preliminary Additive Manufacturing Procedure (pAMP)

ECSS-Q-ST-70-80_1480024

A Preliminary Additive Manufacturing Procedure shall be established in accordance with DRD in Annex B.

The AMP is valid for one machine (one serial number, as per Annex B).

ECSS-Q-ST-70-80_1480025

If a verified AMP is available, the verification may be limited to the new design, in compliance with clause 7.5.

The intent of the AMP is to describe the intrinsic material properties achieved with a defined end-to-end-manufacturing process. Often, this parameter set is applicable for many geometries. Therefore, the AMP can be used for a variety of different part designs.

## Verification on specimen- (AMP), and prototype-level (HFP)

ECSS-Q-ST-70-80_1480026

The AM verification phase shall be split into two phases:

AM verification on metallurgical and mechanical standard test specimens, in compliance with clause 7.4, and

AM verification on prototypes: in compliance with clause 7.5.

ECSS-Q-ST-70-80_1480027

The build job configuration of the prototypes shall be frozen for class 1.1, 1.2 and class 2 parts.

ECSS-Q-ST-70-80_1480028

The build job configuration may be changed for class 3 parts pending approval of the customer.

ECSS-Q-ST-70-80_1480029

Any hardware that is built during the verification phase shall be manufactured in compliance with a previously specified pAMP.

ECSS-Q-ST-70-80_1480030

A-basis design allowables shall be calculated for static tensile properties in accordance with ECSS-E-ST-32 clause 4.5.8.

1	Calculating A-basis design allowables is done before setting the witness sample threshold to ensure that it is sufficiently above these design values.

2	An example on how design allowables can be calculated for a normally distributed population is given in MMPDS chapter 9.4. This meets the intent of calculating A-basis design allowables, considering the requested number of samples in Table 7-2.

ECSS-Q-ST-70-80_1480031

Other approaches than calculating A-basis design allowables specified in requirement 7.3e may be proposed by the supplier, to be agreed with the customer.

Other approaches can be the calculation of B-basis design allowables together with additional justification.

ECSS-Q-ST-70-80_1480032

At the end of the verification phase, the acceptance criteria for material properties for the witness samples to be produced in the hardware production phase, shall be agreed by the supplier and the customer.

## Additive Manufacturing Verification Plan (AMVP)

### Overview

ECSS-Q-ST-70-80_1480033

The supplier shall define an Additive Manufacturing Verification Plan (AMVP) in compliance with Annex C, which allows establishing design allowables for all design driving load types, environments, and failure modes.

ECSS-Q-ST-70-80_1480034

The AMVP specified in 7.4.1a shall be agreed with the customer.

### Safety class 1.1, 1.2, and class 2

ECSS-Q-ST-70-80_1480035

The AMVP for class 1.1, 1.2 and class 2 parts shall include as a minimum the tests listed in Table 7-2.

ECSS-Q-ST-70-80_1480036

For class 1.2 parts, fatigue, and CT scanning need not be performed.

ECSS-Q-ST-70-80_1480037

The design authority shall declare a part to be fatigue critical or not.

ECSS-Q-ST-70-80_1480038

The justification for fatigue criticality from 7.4.2c shall be included in the respective structural analysis report.

ECSS-Q-ST-70-80_1480039

Table 7-2: Test methods for class 1.1, 1.2, and class 2 parts

| Test definition | Characteristics/criteria | Comment |
| --- | --- | --- |
| Visual inspection | See clause 12.3 | On all produced specimens |
| Metallography | See clause 12.5.1 | 6 microsections from specimens evenly distributed in the build volume, covering the full height |
| Tensile testing | See clause 12.5.2 | At least 2 build jobs with 10 valid specimens each (population of minimum 20), evenly distributed in the build volume, from the direction showing the lowest strength values. The supplier is free to build the total number of specimens through a higher number of build jobs. |
| Fatigue testing (not required for class 1.2) | See clause 12.5.3 | For non-fatigue critical hardware: One build job with 12 specimens evenly distributed on the build plate, to create one Wohler curve. For fatigue critical hardware: Two build jobs with 12 specimens each, evenly distributed on the build plate, to create one Wohler curve with 24 data points (testing at least 4 load levels with 6 specimens each) shall be generated. For both cases, the supplier is free to build the total number of specimens through a higher number of build jobs. |
| X-Ray CT | See requirements 12.3g and 12.3h | On fatigue specimens (grip section can be excluded) |
| Powder testing | See clause 13.1 | The powder properties shall be determined if non-virgin powder is used. If virgin powder with a validated CoC is used, no powder testing is required. |
| Customised Tests | To be specified, if requested by the customer. | - |
| NOTE Examples for customised tests are tensile testing with small diameters or thickness to represent thin-walled sections on a part, compression tests for stability sensitive designs, or fatigue crack growth and fracture toughness, tests for fracture control implementation, or tests at high and/or low temperatures. Hardness testing can be useful, if differences in microstructure need to be assessed. |  |  |

### Safety class 3

ECSS-Q-ST-70-80_1480040

A full height blank shall be built, covering the full height of the build job.

ECSS-Q-ST-70-80_1480041

From the bar(s) built in 7.4.3a, 3 samples for micro sectioning shall be extracted.

ECSS-Q-ST-70-80_1480042

Those samples shall be subjected to visual inspection, metallography, or specific application tests specified by the customer.

ECSS-Q-ST-70-80_1480043

The supplier may test 3 tensile specimens evenly distributed in the build volume instead of the requirements 7.4.3a, 7.4.3b and 7.4.3c.

### Reporting

ECSS-Q-ST-70-80_1480044

If all tests were conducted successfully, the pAMP shall become the AMP.

ECSS-Q-ST-70-80_1480045

All test results generated through the AMVP shall be reported in the Additive Manufacturing Verification Report (AMVR) in conformance with the DRD in Annex D.

ECSS-Q-ST-70-80_1480046

All test results shall be incorporated in a Materials Properties Database (MPD), as specified in clause 11.3.1.

The materials database is used to calculate design allowables and can give relevant insight in the repetitiveness of an AM process. The data is not intended to be publicly shared.

## Prototype verification Plan (PVP)

### General

ECSS-Q-ST-70-80_1480047

The supplier shall define a model philosophy in line with the project’s approach for the relevant subsystem.

A Protoflight approach can be an effective way to develop AM hardware, especially for items which are not fatigue critical or safe life potential fracture critical items.

ECSS-Q-ST-70-80_1480048

The supplier shall specify a preliminary Hardware Fabrication Procedure in conformance with the DRD in Annex E.

ECSS-Q-ST-70-80_1480049

The supplier shall specify a Prototype Verification Plan (PVP) in conformance with the DRD in Annex G.

ECSS-Q-ST-70-80_1480050

All prototypes, or test specimens shall be produced in accordance with the preliminary Hardware Fabrication Procedure (pHFP), including all manufacturing steps and post build operations.

### Safety classes 1.1, 1.2, and 2

ECSS-Q-ST-70-80_1480051

A prototype shall be built and tested for every new part design.

Testing of prototypes is done for manufacturing validation.

ECSS-Q-ST-70-80_1480052

Prototypes and witness samples shall be tested as specified in Table 7-3.

ECSS-Q-ST-70-80_1480053

A minimum number of 3 valid tensile test results from witness specimens shall be produced.

It is good practice to plan for a suitable number of spares.

ECSS-Q-ST-70-80_1480054

A Powder capture sample shall be produced to satisfy the requirement in clause 12.2.

ECSS-Q-ST-70-80_1480055

If X-Ray CT is not technically feasible, customised and destructive tests may be required.

ECSS-Q-ST-70-80_1480056

Table 7-3: Test methods for prototypes, and witness samples for safety classes 1.1, 1.2, and 2

| Test definition | Reference | Test object |
| --- | --- | --- |
| Dimensional control | According to drawings | All prototypes, and witness specimens. |
| Visual inspection | See clause 12.3 | 100 %, on all prototypes, and witness specimens, or as far as possible as permitted by the geometrical complexity |
| Tensile witness specimens | See clause 12.5.2 | 3 valid specimens, evenly distributed in the build volume. |
| X-Ray CT | See requirement 12.3g and 12.3h | 100 %, on all prototypes. |
| Density testing | See clause 12.4 | 2 full height blanks. From one, three single sections are extracted. The second one is kept in case a specific volume needs to be assessed. |
| Metallography | See clause 12.5.1 | To be performed on one of the two full height blanks. |
| Powder testing | See clause 13.1 | The powder properties shall be determined if non-virgin powder is used. If virgin powder with a validated CoC is used, no powder testing is required. |
| Powder capture sample | See clause 12.2 | Testing is only done in case of a non-conformance. |
| Customised Tests | To be specified, if requested by the customer. | - |
| NOTE 1 Depending on the requirements for the part, some additional tests can be performed on specific samples: roughness, screws junctions characterizations, pressure test, leak test, particulate contamination, hardness tests and microstructural assessments on selected locations of the produced prototype. NOTE 2 Parts produced with powder bed based methods are prone to show adhering particles on the surface, which can lead to particulate contamination. This occurrence is particularly pronounced for parts produced with electron beam based machines. Cleanliness is usually addressed in the equipment PA requirements. |  |  |

### Safety class 3

ECSS-Q-ST-70-80_1480057

Tests shall be performed in compliance with the Table 7-4.

ECSS-Q-ST-70-80_1480058

Density testing, as required in Table 7-4 may be replaced by tensile testing of 3 specimens.

ECSS-Q-ST-70-80_1480059

Table 7-4: Test methods for prototypes, and witness specimens for safety class 3

| Test definition | Reference | Test object |
| --- | --- | --- |
| Dimensional control | According to drawings | All prototypes, and witness specimens. |
| Visual inspection | See clause 12.3 | 100 %, on all prototypes, and witness specimens, or as far as possible as permitted by the geometrical complexity. |
| Density testing | See clause 12.4 | 2 full height blanks. From one, three single sections are extracted. The second one is kept in case a specific volume needs to be assessed. |
| Powder capture sample | See clause 12.2 | Testing is only done in case of a non-conformance. |
| Customised Tests | To be specified, if requested by the customer. | - |

### Reporting

ECSS-Q-ST-70-80_1480060

The pHFP shall become the HFP after all tests were conducted successfully.

ECSS-Q-ST-70-80_1480061

All test results generated through the PVP shall be reported in the Prototype Verification Report (PVR) in accordance with Annex H.

ECSS-Q-ST-70-80_1480062

The test results of the witness specimens shall be incorporated in a Materials Properties Database (MPD), in accordance with clause 11.3.1.

## Re- verification of AM machines

### Overview

Re-verification is necessary, if modifications on an existing and verified machine are performed.

### Requirements

ECSS-Q-ST-70-80_1480063

All tests in the AMVP shall be repeated, if major software or hardware updates were performed which can impact the processing parameters.

ECSS-Q-ST-70-80_1480064

For safety class 1.1, 1.2, and 2, all tests in Table 7-2, with the exception of customised tests and fatigue tests, shall be repeated, if:

A machine was re-located;

Essential components were replaced, repaired, or altered;

Minor software updates were performed which do not impact the processing parameters;

The AM machine has not been operated for 6 months or more.

1	Essential components can be the laser or the scanner head, or any other part which is crucial to reach the required laser beam quality. A non-essential component could be a recoater blade, which is considered to be a consumable.

2	Software affected by these requirements is any, which can affect the processing parameters of the AM machine.

## Machine pause

### Overview

A machine pause is a stop of beam with no other associated phenomenon such as a stop of heating system, power outage, collision of recoater with the part, or loss of inert atmosphere.

### Requirements

ECSS-Q-ST-70-80_1480065

No unplanned process interruption shall be accepted during the verification phase.

An unplanned process interruption can be triggered by a stop of heating system, power outage, collision of recoater with the part, loss of inert atmosphere, scheduled or un scheduled maintenance, etc.

ECSS-Q-ST-70-80_1480066

Unplanned process interruptions may be acceptable upon customer agreement during the verification phase, if the elapsed time is less than the elapsed time between two consecutive layers.

ECSS-Q-ST-70-80_1480067

If a machine pause is planned to occur during the hardware production phase, dedicated tests to characterise the properties of the interface zone shall be included in the AMVP.

ECSS-Q-ST-70-80_1480068

For planned machine pauses, a procedure for re-start shall be established by the supplier and agreed with the customer.

ECSS-Q-ST-70-80_1480069

The recommendations of the OEM regarding machine restart shall be followed.

## Repair

ECSS-Q-ST-70-80_1480070

No repair of the manufactured part(s) or specimens shall be permitted during the verification phase.

## Manufacturing supports

ECSS-Q-ST-70-80_1480071

Prototypes or standard test samples shall be free of any residues of supports, if the prototypes or test samples are tested without subsequent machining.

## Parts cleaning

ECSS-Q-ST-70-80_1480072

Cleaning processes shall be applied so that the parts comply with cleanliness requirements of the equipment.

Particulate contamination (PAC) can e.g. occur due to particles adhering to the part’s surface. Molecular contamination (MOC) can e.g. include residues of cutting fluids for milling or turning.

## Documentation

ECSS-Q-ST-70-80_1480073

The AMVP and the PVP shall be incorporated in the first issue of the RFA in accordance with Annex D of ECSS-Q-ST-70.

See also Figure 4-1.

ECSS-Q-ST-70-80_1480074

The AMVR and the PVR shall be incorporated in the second issue of the RFA in accordance with Annex D of ECSS-Q-ST-70.

See also Figure 4-1.

## Manufacturing Readiness Review (MRR)

ECSS-Q-ST-70-80_1480075

The MRR shall be performed in compliance with ECSS-Q-ST-20.

ECSS-Q-ST-70-80_1480076

The results of the verification testing, AMVR and PVR, and the HFP shall be presented at MRR.

ECSS-Q-ST-70-80_1480077

The second issue of the RFA shall only be approved after having successfully performed the MRR.

ECSS-Q-ST-70-80_1480078

During the MRR, it shall be confirmed to the customer that build job configuration is under configuration control.

# Hardware production

## Overview

The aim of this phase is to produce the intended hardware according to the previously defined HFP, and to validate it through non-destructive, mechanical, or functional tests, as well as through witness specimens.

## Requirements for hardware production

### General

ECSS-Q-ST-70-80_1480079

Hardware production shall be done in compliance with the Hardware Fabrication Procedure (HFP) from the DRD in Annex E.

ECSS-Q-ST-70-80_1480080

The supplier shall produce and test the witness specimens according to Table 8-1.

ECSS-Q-ST-70-80_1480081

Table 8-1: Overview of witness samples to be produced with hardware

| Test object | Safety Class 1.1 | Safety Class 1.2 | Safety Class 2 | Safety Class 3 |
| --- | --- | --- | --- | --- |
| Tensile test specimens | 3 | 3 | 3 | 3 tensile specimens or 1 full height blank |
| Full height blanks | 2 | 2 | 1 |  |
| Powder Capture Sample | 1 | 1 | 1 | - |

### Process interruption

ECSS-Q-ST-70-80_1480082

If an unplanned process interruption occurs during the hardware production phase, the manufacturer may continue the manufacturing.

ECSS-Q-ST-70-80_1480083

In case of an unplanned process interruption specified in requirement 8.2.2a, a major nonconformance shall be raised.

### Manufacture of hardware and witness samples

#### Overview

Witness samples produced with hardware provide a reference of the material properties within the produced build job. An overview of the different witness samples and test methods is given in Table 8-1.

#### Standard tensile test specimens

ECSS-Q-ST-70-80_1480084

Samples to provide validation of material shall be built as test pieces and undergo all post processing steps as specified in the HFP.

ECSS-Q-ST-70-80_1480085

The shape and orientation of the specimens shall be determined in compliance with clause 12.5.2.

ECSS-Q-ST-70-80_1480086

The tensile specimens shall be evenly distributed in the build volume.

ECSS-Q-ST-70-80_1480087

In case overlapping areas are present in the part, the arrangement of the specimens shall cover all combinations of lasers for multi laser systems including overlapping areas.

It is best practice to place the tensile test specimen such that the maximum height of the FM is in the gauge length.

ECSS-Q-ST-70-80_1480088

A minimum number of 3 valid tensile test results shall be produced for all safety class 1.1, 1.2, and 2.

It is good practice to plan for a suitable number of spares.

#### Full height blanks

ECSS-Q-ST-70-80_1480089

The full height blanks shall undergo the same post processing steps as defined in the HFP for the part.

ECSS-Q-ST-70-80_1480090

The full height test blanks shall reach at least the same height as the part.

#### Powder capture sample

ECSS-Q-ST-70-80_1480091

Powder capture samples shall be produced in compliance with clause 12.2.

## Testing of witness samples

### Tensile testing

ECSS-Q-ST-70-80_1480092

All tensile tests shall be performed in compliance with clause 12.5.2.

ECSS-Q-ST-70-80_1480093

The yield strength, tensile strength, elastic modulus, and elongation at break of each individual tensile test shall all be within the ranges specified in the PVP.

### Full height blanks

#### Safety class 1.1 and 1.2

ECSS-Q-ST-70-80_1480094

The density shall be measured on the full height blanks in compliance with clause 12.4.

ECSS-Q-ST-70-80_1480095

The second full height blank shall be stored and only be tested, if needed for a failure investigation.

These are necessary to provide material for inspection if a build interruption occurs. One full height blank can be inspected at the height of the process interruption to assess its impact on the as-built microstructure.

ECSS-Q-ST-70-80_1480096

Metallography shall be performed for class 1.1 and 1.2 parts on the full height blanks in accordance with clause 12.5.1.1.

ECSS-Q-ST-70-80_1480097

The chemical composition including light elements shall be assessed on the full height blanks for class 1.1 and 1.2 parts.

1	If during the AM-pre-verification phase, a feedstock and recycling study demonstrates negligible change in composition within the specified limits, then chemical composition specimens are expected to be less critical.

2	For feedstock/process combinations which show, for example, a continuous increase in O content or a continuous decrease in Mg content to a specified limit, then, determining the chemical composition can be done in all builds and analysed before part release.

#### Safety class 2 and 3

ECSS-Q-ST-70-80_1480098

The density shall be measured in compliance with clause 12.4.

### Powder capture sample

ECSS-Q-ST-70-80_1480099

The powder capture sample shall be removed from the baseplate before any heat treatment or HIP process.

ECSS-Q-ST-70-80_1480100

The powder capture sample shall be stored and only be tested in accordance with clause 13.1, if needed for a failure investigation.

ECSS-Q-ST-70-80_1480101

The powder capture sample specified in 8.3.3b, may be analysed immediately to avoid storing.

## Inspection of hardware

### Non-destructive techniques

ECSS-Q-ST-70-80_1480102

The supplier shall implement at least the non-destructive tests in accordance with Table 8-2.

If the part is under fracture control, more NDT can be needed, to satisfy ECSS-E-ST-32-01. For NDT see ECSS-Q-ST-70-15.

ECSS-Q-ST-70-80_1480103

The NDT methods in Table 8-2 shall be carried out in accordance with clause 12.3.

ECSS-Q-ST-70-80_1480104

The part shall be accepted if the found indications are in compliance with the acceptance criteria specified in the PVP.

ECSS-Q-ST-70-80_1480221

Table 8-2: Overview of non-destructive tests for AM hardware

| Test definition | Safety Class 1.1 | Safety Class 1.2 | Safety Class 2 | Safety Class 3 |
| --- | --- | --- | --- | --- |
| X-Ray CT | 100 % | 100 % | - | - |
| Visual inspection | 100 %, or as far as possible as permitted by the geometrical complexity of the part | 100 %, or as far as possible as permitted by the geometrical complexity of the part | 100 %, or as far as possible as permitted by the geometrical complexity of the part | 100 %, or as far as possible as permitted by the geometrical complexity of the part |
| Dimensional control | 100 % | 100 % | 100 % | Sampling according to ISO 2859-1:1999 sensitivity level II, AQL 0.65 |
| Functional test or proof test | If no X-Ray technique is technically feasible or useful | If no X-Ray technique is technically feasible or useful | - | - |

ECSS-Q-ST-70-80_1480105

If required in Table 8-2 for the respective safety class, X-Ray CT testing shall be performed after the last heat- or HIP-treatment.

ECSS-Q-ST-70-80_1480106

The X-Ray CT Testing, specified in 8.4.1d, may be performed before a final machining step.

ECSS-Q-ST-70-80_1480107

If required in Table 8-2 for the respective safety class, visual inspection, dimensional control, and functional tests shall be performed after the last post-processing step.

It is best practice to perform selected NDT techniques after each manufacturing step to mitigate the production risk in addition to the tests in requirement 8.4.1d and f.

ECSS-Q-ST-70-80_1480108

For class 1.1 and 1.2 parts, functional tests may be performed instead of X-Ray techniques if these are technically not feasible.

Examples of parts that cannot be inspected with X-Ray techniques include ones that cannot be penetrated due to their size, thickness, or the material’s density.

ECSS-Q-ST-70-80_1480109

X-Ray CT may be replaced by 2D X-Ray inspection if agreed with the customer.

## Reporting

ECSS-Q-ST-70-80_1480110

All test results of clause 8.3 and 8.4 shall be reported in the Hardware Production Report (HPR) in conformance with the DRD in Annex F.

# AM operation and supervision personnel

## Overview

The aim of this clause is to ensure the suitability of operating and supervision personnel.

It is best practice that the positions described in clauses 9.2-9.4 are not held by one person only to avoid a single point of failure.

## AM supervisor

ECSS-Q-ST-70-80_1480111

The appointment of the AM supervisor shall be reported to the customer.

ECSS-Q-ST-70-80_1480112

The manufacturer shall employ an Additive Manufacturing supervisor who is responsible for the following tasks:

Facility and equipment maintenance,

Health and safety,

The AMP,

Build job configuration.

1	The AM supervisor does not necessarily have to personally perform the tasks listed in requirement 9.2b, but is expected to supervise and record these tasks.

2	Facility and equipment maintenance also includes software maintenance of the AM equipment.

## Qualification and certification of AM operators

### Laser based Powder Bed Fusion processes

ECSS-Q-ST-70-80_1480113

Only operators holding a valid qualification test certificate for Laser Powder Bed Fusion (L-PBF) in compliance to ISO ASTM 52942:2020 shall perform operations on such equipment.

### Electron Beam based Powder Bed Fusion processes

ECSS-Q-ST-70-80_1480114

The supplier shall define a training and test program for qualifying machine operators of electron beam metal powder bed fusion machines and equipment.

At the time of issuing this standard, no dedicated standard for qualifying E-PBF operators was available. ISO ASTM 52942:2020 was developed for laser beam based machines, but can be used as reference when meaningfully applied.

ECSS-Q-ST-70-80_1480115

Only operators holding a valid qualification test certificate in accordance with requirement 9.3.2a shall perform operations on electron beam based powder bed fusion equipment.

## Qualification and certification of personnel for NDT

ECSS-Q-ST-70-80_1480116

Personnel performing Non-Destructive Testing on additively manufactured parts shall be trained and certified in accordance with ECSS-Q-ST-70-15.

## Safety of Personnel

ECSS-Q-ST-70-80_1480117

National regulations applicable for operators of metal powder bed fusion equipment shall be applied.

ECSS-Q-ST-70-80_1480118

If such national regulations are not available, the supplier shall implement safety measures for personnel by himself.

# Equipment and facilities

## Overview

The aim of this clause is to ensure the suitability of the applied equipment and the used facilities.

## Conditions for facilities

ECSS-Q-ST-70-80_1480119

The temperature of the room where the AM machine is operated shall always be between 20 °C and 25 °C with a maximum relative humidity of 50 %, if powders are exposed to this environment.

## Laser based equipment calibration

ECSS-Q-ST-70-80_1480120

The acceptance inspection shall be performed in accordance with to ISO ASTM 52941:2020.

## Electron beam based equipment calibration

ECSS-Q-ST-70-80_1480121

          - The acceptance inspection shall be performed in accordance with OEM specification.

### Frequency

ECSS-Q-ST-70-80_1480122

Beam calibration shall be performed in the following cases:

Scheduled in maintenance program,

Machine has been moved,

Differences have been observed between parts,

Changes of machine hardware have been done.

ECSS-Q-ST-70-80_1480123

Beam calibration shall ensure that the spot quality is equal over the entire build area.

### Calibration protocol description

ECSS-Q-ST-70-80_1480124

Automatic calibration procedure shall be performed in accordance with OEM equipment handbook.

ECSS-Q-ST-70-80_1480125

Verification of calibration shall be performed as follows:

Building of OEM verification plate, which achieve a beam test pattern.

Check the beam calibration plate status with visual inspection, which allows evaluation of:

Dimensional accuracy of bead

Beam alignment

Focus offset

Electron beam deflection system

Building of OEM reference part in order to finalise evaluation of:

Dimensional accuracy of shape

Material properties

## Maintenance and repair

### Maintenance of laser based machines

ECSS-Q-ST-70-80_1480126

As a minimum, maintenance shall be carried out as described in the OEM equipment handbook.

ECSS-Q-ST-70-80_1480127

In the absence of clear OEM instructions, maintenance activities shall include:

After each build

Visual inspection of the system,

Check of laser-protection glass in the process chamber door and process chamber cover (contamination, scratches, penetration, etc.),

Clean laser glass,

Check recoater condition,

Check gas circulation filter and change if necessary,

Weekly

Check of safety equipment (emergency stop, etc.),

Visual check and, if polluted, cleaning of gas outlet valve,

Check filter on personal protection for impurities and clean or replace if polluted,

Check filter on cooling unit and clean or replace if polluted,

Check coolant filling level and fill it if level is low,

Check cooling water for impurities,

Check DI cartridge on cooling unit and clean or replace if necessary.

Monthly

Clean areas behind removable inner walls, if they are present,

Testing emergency shutdown, emergency stop,

Check the sieving equipment for damage

Half-yearly

Change cooling water.

Annually

Check fire extinguisher,

Check, clean and calibrate optical systems,

Clean gas circulation pipes,

Check mechanical drives, guides and bearings,

Check seals,

Inspect air dryer and filters.

ECSS-Q-ST-70-80_1480128

All maintenance records shall be noted in an equipment log book, either digitally or on paper.

### Maintenance of electron beam based machines

ECSS-Q-ST-70-80_1480129

As a minimum, maintenance shall be carried out as described in OEM equipment handbook.

ECSS-Q-ST-70-80_1480130

Maintenance activities shall include:

After each build

Check log and analyse results from build done,

Visual inspection of the system,

Vacuum clean the powder basin centre area with clean vacuum cleaner,

Check the chamber interior for metallisation and clean if polluted,

Check or change protections foils of beam column, chamber,

Check or change observation window protection glass,

Vacuum clean the chamber from loose particles with dirty vacuum cleaner,

Remove tank and sandblast cake in dedicated sandblaster,

Sieve powder contents in sandblaster and clean vacuum cleaner,

Fill hoppers with sieved powder,

Clean seals and door,

Close the chamber and start vacuum.

Before a build

Check that the rake is properly attached and the condition of rake teeth,

Check amount of powder according to height of next job,

Check or trim the powder dispatcher in accordance with OEM equipment handbook.

Weekly

Check of safety equipment,

Check filter on personal protection for impurities and clean or replace if polluted,

Clean floor of laboratory.

Monthly

Clean areas: Cabinet, computer, behind the side walls,

Check coolant filling level and fill it if level is low,

Check Helium filling level and fill it if level is low,

Testing emergency shutdown, emergency stop,

Check / clean the sieving equipment for damage.

Yearly

Check fire extinguisher,

Inspect air dryer and filters,

Inspect sandblaster and change filters.

A – Maintenance: See OEM handbook for frequency

Check electron beam unit: cathode, top column, sensors,

Check vacuum chamber,

Check camera system,

Check mechanical drives, guides and bearings,

Check / adjust powder dispatcher system,

Check seals.

B – Maintenance: See OEM handbook for frequency

Change cathode,

Check electron beam unit: top column, sensors,

Check vacuum chamber,

Check camera system,

Check mechanical drives, guides and bearings,

Change rake arm,

Check / adjust powder dispatcher system,

Check / adjust build tank and table,

Check seals.

Safety equipment can refer to devices which trigger e.g. emergency stops, etc.

ECSS-Q-ST-70-80_1480131

All maintenance records shall be noted in an equipment log book, either digital or paper.

### Repair

ECSS-Q-ST-70-80_1480132

All repairs shall be noted in an equipment log book.

ECSS-Q-ST-70-80_1480133

After each repair, follow-up actions shall be performed as specified in the OEM handbook.

ECSS-Q-ST-70-80_1480134

In case of doubt, the follow-up action shall be mutually agreed with the OEM.

## Materials and consumables

### Management of powder

ECSS-Q-ST-70-80_1480135

The manufacturer shall produce a Powder Management Plan in conformance with DRD in Annex I for approval by the customer.

ECSS-Q-ST-70-80_1480136

For safety class 1.1, class 1.2 and 2, only alloys of the same family shall be processed in the same build chamber due to the risk of cross-contamination.

1	Examples of families of alloys commonly used by the space industry are:

Nickel based alloys as IN 718, IN 625, and Hastelloy X

Aluminium alloys as AlSi10Mg, AlSi7Mg0.6, AA8009, and Scalmalloy®

Ferritic stainless steels and martensitic stainless steels

Austenitic stainless steels and Nickel containing iron alloys as INVAR®

Titanium alloys containing more than 85 weight-% titanium as Ti-6Al-4V

2	Austenitic stainless steels are not considered to be of the same family of ferritic or martensitic stainless steels.

### Tooling and features

ECSS-Q-ST-70-80_1480137

Bottles, funnels, sieves and hand tools shall be dedicated to one family of alloys

ECSS-Q-ST-70-80_1480138

Cleaning of solid surfaces of tools or any other manufacturing equipment shall be carried out with a wipe and IPA.

### Gases

ECSS-Q-ST-70-80_1480139

The purity of argon shall be at least 99,998 %.

ECSS-Q-ST-70-80_1480140

The purity of nitrogen shall be at least 99,998 %.

ECSS-Q-ST-70-80_1480141

Nitrogen shall not be used with Ti-alloys.

### Cleaning of machines

ECSS-Q-ST-70-80_1480142

In addition to cleaning of mPBF machines in line with maintenance schedules, cleaning of the powder path shall be carried out after completion of the maximum number of validated powder recycles.

# Quality assurance

## Configuration control

ECSS-Q-ST-70-80_1480143

The AMP and the HFP shall be under configuration control.

## Maintenance of AM procedure

### Overview

The basic principle is that as soon an AMP or a HFP has been verified, no modification is permitted without customer agreement. Changes of these procedures may require partial or complete re-verification.

### Requirements

ECSS-Q-ST-70-80_1480144

Every modification of a verified AMP or HFP shall be agreed between supplier and customer and the documents updated accordingly.

## Statistical Process Control

### Materials Properties Database (MPD)

ECSS-Q-ST-70-80_1480145

A MPD shall be populated with data, generated from one AMP.

Data from witness specimens which have been produced according to an AMP can also be included in the MPD. An example of a MPD is given in Annex K.

ECSS-Q-ST-70-80_1480146

Data shall only be included in the MPD, if it is produced with a verified AMP.

ECSS-Q-ST-70-80_1480147

Data shall only be included, if it is considered to be “in family” of the existing material property suite.

ECSS-Q-ST-70-80_1480148

A dataset shall only be considered “in family” with an existing materials property suite, if the deviation of the arithmetic average of the yield and tensile strength does not exceed three standard deviations.

Typically, the “in family” criterion is only applied for static mechanical properties.

## Quality control

### Reference and witness samples

ECSS-Q-ST-70-80_1480149

Witness samples shall be stored in conformance with life duration of the mission upon customer request.

### Documentation of manufacturing

ECSS-Q-ST-70-80_1480150

Traceability shall be ensured through a shop traveller.

The shop traveller can include the dates of the different manufacturing steps including post operations, the powder batch number, the powder level in machine before start, confirmation of compliance with AMP through operator’s signature, etc.

ECSS-Q-ST-70-80_1480151

All data shall be available for review.

### Anomalies and non-conformances occurring during the AM process

ECSS-Q-ST-70-80_1480152

In case of anomalies occurring during the AM process, a nonconformance report in compliance with ECSS-Q-ST-10-09 shall be raised.

A deviation from the qualified range of one or more process parameters can be considered as anomalies.

## Auditing

ECSS-Q-ST-70-80_1480153

A supplier process audit shall be performed for new suppliers prior to the start of the pre-verification phase.

ECSS-Q-ST-70-80_1480154

Suppliers may be re-audited if major changes to the end-to-end manufacturing process are made.

An example of an audit check list is proposed in Annex J.

## End Item Data Pack

ECSS-Q-ST-70-80_1480155

The EIDP shall be created in compliance with Annex B of ECSS-Q-ST-20.

# Testing of AM materials and parts

## Overview

The aim of this clause is to detail several non-destructive and destructive testing methods which are called up through the above requirements.

## Powder capture sample

### Overview

Powder capture samples provide a useful historic reference to a powder used in a build. They can also provide an indication of any powder contamination issue occurring before or during the build.

A powder capture sample can be an mPBF container built during the mPBF which intrinsically contains powder as-supplied to the build chamber and any contaminants generated during the build.

Equally, it can be a powder sampling tool, which is inserted into the bed, collects a sample and is then withdrawn.

### Requirement

ECSS-Q-ST-70-80_1480156

Powder capture samples shall contain sufficient powder for any likely retrospective tests.

## NDT for AM

ECSS-Q-ST-70-80_1480157

The selection of NDT techniques shall be performed in the AM definition phase and implemented in accordance with ECSS-Q-ST-70-15.

ASTM E3166:2020 “Standard Guide for Non-destructive Examination of Metal Additively Manufactured Aerospace Parts After Build” can be used complementary for examining AM parts.

ECSS-Q-ST-70-80_1480158

Visual inspection shall be performed in compliance with ECSS-Q-ST-70-15.

ECSS-Q-ST-70-80_1480159

Visual inspection shall be performed after completion of the build job and after separation from the build plate.

It is best practice to carry out the visual inspection with a magnification of 10x or higher. The aim of the visual inspection is to locate any superficial anomalies. This can include cavities, discolouration, contamination, cracks, lack of fusion, and as far as this can be detected with the applied magnification.

ECSS-Q-ST-70-80_1480160

Dye penetrant inspection shall be performed if specified by the customer.

ECSS-Q-ST-70-80_1480161

Dye penetrant inspection shall be carried out with sensitivity level 2 in accordance with AMS 2644, unless otherwise specified by the customer or necessary for implementation of for example fracture control.

For example, fracture control requirements can ask for a higher sensitivity level than 2 or even a different technique.

ECSS-Q-ST-70-80_1480162

The dye of the selected method shall be cleanable in full.

AM parts are expected to have relatively high surface roughness, which makes dye penetrant inspection challenging to apply. Jet-, vapour-, and bead-blasting can close surface-cracks and it is therefore best practice to apply an etch before dye penetrant inspection.

ECSS-Q-ST-70-80_1480163

X-Ray CT shall be applied to detect internal defects in accordance with ASTM E 1570 and ASTM E 1441 unless otherwise specified.

Typical internal defects for mPBF processes are pores, lack of fusion, cracks, or inclusions. X-Ray CT can also provide the porosity level, the defect’s size, shape, and location.

ECSS-Q-ST-70-80_1480164

For X-Ray CT, the voxel size shall be adapted to the smallest acceptable defect size.

It is best practise to adjust the resolution such that the smallest acceptable defect size can be detected with at least two voxels. Other important parameters include the contrast to noise ratio, the focal spot size, the reference samples for detection of smallest defect size, etc.

ECSS-Q-ST-70-80_1480165

In cases where the acceptance criteria for inner defects cannot be verified with NDT techniques, the supplier shall propose and justify an alternative method to assess these.

Alternative methods can include process monitoring techniques or proof testing.

## Density testing

### Overview

State of the art AM processes can show some porosity in the form of lack of fusion-like defects and/or pores. The relative density of AM material is therefore a crucial factor to judge its “health”, and it is often measured with “full height blanks”. A full height blank is a free-standing specimen that stretches from the base plate to the maximum height of the part to be built and can have a circular (typically Ø 10 mm) or a rectangular (typically 10x10 mm2) cross section.

### Requirements

ECSS-Q-ST-70-80_1480166

          - Density specimens produced together with a part shall not be positioned farther away from the actual part than 20 mm in x or y direction.

ECSS-Q-ST-70-80_1480167

          - At least one sample shall be positioned at the side where the gas is extracted from the build chamber and tested.

Techniques for density measurement include Archimedes (EN ISO 3369:2010 or ASTM B 962:2017), X-ray CT, and quantitative metallography.

## Destructive testing

### Metallography

#### General Metallography

ECSS-Q-ST-70-80_1480168

Microsections shall be made normal to the Z-axis, in accordance with clause 5.1, to evaluate bulk material and parallel to the Z-axis, for the assessment of melt pool characteristics.

ECSS-Q-ST-70-80_1480169

The microstructure shall be demonstrated free of unacceptable defects when evaluated with metallurgical cross-sections at a minimum magnification of 50x and an area of evaluation ≥ 1cm2.

1	Detrimental defects can include foreign particle inclusions, or pores, lack of fusion or cracks, exceeding defined acceptance criteria.

2	The basic concept of microstructural investigations for AM material was adopted from NASA MSFC-SPEC-3717.

ECSS-Q-ST-70-80_1480170

In case of utilising more than one beam, it shall be demonstrated that this results in consistent mechanical properties throughout the build area, including the regions where beams overlap.

“beams” includes laser and electron beams.

ECSS-Q-ST-70-80_1480171

Grain size and morphology shall be assessed qualitatively through metallography.

ECSS-Q-ST-70-80_1480172

For class 1.1 and 1.2, the chemical composition shall be determined.

ECSS-Q-ST-70-80_1480173

The presence of any alpha case layer on the surface of titanium alloys shall be determined in compliance with EN 2003-009:2007.

ECSS-Q-ST-70-80_1480174

For parts in compliance with safety class 1.2 and class 3, alpha case on Ti-6Al-4V may be accepted without measurement, if the stresses with applicable margins are below 100 MPa.

Thick alpha case layers can release particles, which needs to be avoided.

ECSS-Q-ST-70-80_1480175

No alpha case shall be accepted for any safety class and Ti-6Al-4V, if stresses with applicable margin above 100 MPa, unless technically justified and agreed by the customer.

#### Top and bottom layer melt pool assessment

ECSS-Q-ST-70-80_1480176

The assessment shall include blanks from the bottom of the build and the top of the build for the characterisation of the top layer melt pool.

ECSS-Q-ST-70-80_1480177

The top surface layer of each blank shall be sectioned parallel to the Z-axis for the assessment of the melt pool of this layer.

ECSS-Q-ST-70-80_1480178

Any cosmetic or smoothing pass shall be omitted during the manufacture of these samples.

Top layer melt pool blanks are useful for the inspection of the geometry and macrostructure of melt tracks. Therefore a top (surface) layer from the bottom of the build is compared with a top (surface) layer at the top of the build in order to confirm laser and optics performance at the beginning and end of the build, and to validate against material produced during different builds. Please note that some mPBF equipment nominally apply a cosmetic or smoothing pass on top surfaces. The melt pool assessment is intended to show the typical process result without this cosmetic or smoothing pass.

ECSS-Q-ST-70-80_1480179

To evaluate the repeatability of the machine, the arithmetic average of the depth of a full melt pool (dP) to layer thickness (tL), and the depth of the overlap (dO) to layer thickness (tL), shall be calculated from at least 10 melt pools from the top and the bottom of the build.

1	The concept of investigating the top layer melt pool, including the approach of melt pool measurements, as also shown in Figure 12-1 were adopted from NASA MSFC-SPEC-3717.

2	The measurements taken during top surface Melt Pool evaluation are used to check repeatability of the machine using a defined set of parameters, see Figure 12-1. tL = defined nominal layer thickness, dP = depth of full melt pool, dO = depth of overlap (between adjacent melt pools). There is no acceptance criteria; this measurement sets the baseline for the performance of the individual machine and parameter set.

Figure 12-1: Melt pool measurement concept [Image and concept: adopted from NASA MSFC-SPEC-3717]

### Tensile testing

ECSS-Q-ST-70-80_1480180

The direction showing the lowest strength values, determined within the pre-verification phase, shall be tested.

1	The direction showing the lowest strength values is often Z (vertical).

2	Additional justification that the tested samples represent the worst case properties at critical locations can be provided by, for example metallurgical and hardness investigations of flight representative hardware.

ECSS-Q-ST-70-80_1480181

The tensile tests shall be performed in accordance with ECSS-Q-ST-70-45.

Values of the elastic modulus can vary to some extent if determined through tensile testing, and it can be necessary to define wider ranges for the acceptance criteria.

ECSS-Q-ST-70-80_1480182

The surface condition of the tensile specimens shall be proposed by the supplier and agreed with the customer.

ECSS-Q-ST-70-80_1480183

The elongation at break shall be above 8 % for Ti-6Al-4V.

1	A martensitic microstructure is usually achieved when producing Ti-6Al-4V materials through Laser Powder Bed Fusion processes. Heat treatments can alter this to an - microstructure. Titanium martensite generally affects the mechanical properties such that strength values would increase and toughness or ductility values would decrease. It is therefore strongly recommended to apply heat treatments (e.g. at about 800 °C) to transform martensite into an - microstructure.

2	Other alpha-beta titanium alloys may exhibit similar challenges regarding heat treatments on secondary mechanical properties and it is therefore recommended to consider this effect.

### Fatigue testing

#### Overview

Parts produced with Laser Powder Bed Fusion processes generally exhibit a rather high surface roughness, have residual stresses, and a varying microstructure throughout the build height. These features are known to have an effect on the fatigue performance.

#### Requirements

ECSS-Q-ST-70-80_1480184

The fatigue tests shall be performed in accordance with ECSS-Q-ST-70-45.

ECSS-Q-ST-70-80_1480185

The orientation of the fatigue specimens shall be proposed by the supplier for acceptance by the customer.

ECSS-Q-ST-70-80_1480186

The surface condition of the fatigue specimens shall be proposed by the supplier and accepted by the customer.

1	It is best practice to test the fatigue specimens in a representative surface condition, according to the end to end manufacturing process, defined in the AMP.

2	Surface treatments can include jet blasting, electro polishing, and plasma polishing or similar processes.

ECSS-Q-ST-70-80_1480187

The load ratio (R) shall be representative of the final application.

In many cases, a stress ratio of -1 is representative of space applications, especially when the dominant load is caused by vibration.

# Powders

## Testing of powders

ECSS-Q-ST-70-80_1480188

          - With a test method proposed by the supplier and agreed with the customer, testing of powders shall include as a minimum:

            - Chemical composition, including light elements,

            - Particle size distribution,

            - Density in both apparent and tapped conditions, and

Flow properties.

1	For requirement 13.1a1: light elements can include carbon, hydrogen, oxygen, and nitrogen.

2	For requirement 13.1a1: the chemical composition can be determined by energy-dispersive spectrometry (EDS) as per ISO 22309:2011 or ASTM E1508 or by atomic emission spectrometry for Aluminium alloys as per ASTM E3061:2017 and for titanium alloys as per ASTM E 2371:2013.

3	For requirement 13.1a1: determination of hydrogen in titanium alloys can be done by inert gas fusion as per ASTM E 1447:2016. Determination of carbon in refractory and reactive metals can be done by combustion analysis as per ASTM E 1941:2016. Determination of oxygen in titanium alloys can be done by reduction-extraction methods as per ISO 4491-4:2019. Oxygen and nitrogen in titanium alloys can be determined by inert gas fusion as per ASTM E 1409:2013.

4	For requirement 13.1a1: increased oxygen content can lead to reduced ductility of IN 718 at elevated temperatures. It is best practice to limit the oxygen content in the base material more strictly than this is done for conventional materials.

5	For requirement 13.1a2: particle size distribution can be analyzed by sieve analysis as per ISO 4497:2020 or ASTM B214:2016, by laser diffraction in compliance with ISO 13320:2020 or ASTM B822:2017 or by image analysis in compliance with ISO 13322:2014.

6	For requirement 13.1a3: the apparent density can be determined according to ISO 3923-1:2018 or ASTM B212:2017 (Funnel Method). The tap density can be determined according to ISO 3953:2011 or ASTM B527.

7	For requirement 13.1a3: testing for porosity in powder particles is not required, but it can be performed by helium pycnometry in compliance with ASTM B923:2020, or through X-Ray CT scanning.

8	For requirement 13.1a4: flow properties can be determined through the Hall Flowmeter test in compliance with ASTM B213:2020, ASTM B 964:2016, or ISO 4490:2018 and tap density as per ASTM B527:2020. Alternatively, “angle of repose” tests according to ISO 4324:1977 can also be used.

9	For requirement 13.1a4: it is best practice to determine powder particle morphology and satellite build-up with an SEM as complementary information.

10	Aluminium powders are known to pick up moisture, which can degrade flow properties or lead to significant gas porosity in the final AM part. It is best practice to control the humidity level in areas where AM powder is handled or stored. The test can be performed using one of the following methods: capacitive titration (Karl-Fischer) according to ISO 760:1978 or ASTM E203:2016, thermogravimetric according to ASTM E1131:2020, or with a humidity sensor.

## Procurement

ECSS-Q-ST-70-80_1480189

          - The procurement specification shall include limits of properties specified in 13.1a.

ECSS-Q-ST-70-80_1480190

The chemical composition shall be in compliance with national or international standards if these are available.

Examples include: ASTM F3001:2014 for Ti6Al4V ELI, ASTM F2924:2014 for Ti6Al4V, ASTM F3318:2018 for AlSi10Mg, ASTM F3055:2014 for nickel alloy 718, ASTM F3184:2016 for SS316, ASTM F3056:2014 for nickel alloy 625.

ECSS-Q-ST-70-80_1480191

The certificate of conformance (CoC) shall include measurement values for the properties specified in 13.1a.

ECSS-Q-ST-70-80_1480192

The CoC shall clearly indicate whether the powder meets the procurement specification.

ECSS-Q-ST-70-80_1480193

When delivered from the supplier, all powder shall be in a sealed powder container with a witness tag between the lid and container to prove it has not been opened.

## Safe Handling

ECSS-Q-ST-70-80_1480194

          - Powders shall be handled in line with national or European occupational health regulations.

AM Powders require careful handling. They can be flammable and hazardous and pose a danger to health if handled incorrectly.

## Storage

ECSS-Q-ST-70-80_1480195

          - The container shall be labelled with the contents, the batch number, and the date of storage beginning.

ECSS-Q-ST-70-80_1480196

          - Powder, containers shall be stored in humidity and temperature controlled area.

ECSS-Q-ST-70-80_1480197

Powders shall be stored in compliance with national or European occupational health regulations.

## Loading

ECSS-Q-ST-70-80_1480198

          - Loading of powder shall follow machine-specific instructions.

## Recycling

ECSS-Q-ST-70-80_1480199

          - The use of recycled powder shall be permitted once a validation of mPBF recycled powder is demonstrated to show properties within the limits specified in clause 13.2a.

1	Efficient production using mPBF processes can require recycling of power. Recycled powder arises from excess powder removed by the recoater arm and un-fused powder from a build process.

2	This applies to mPBF equipment with and without automated powder re-cycling systems.

3	It is common practice to submit a powder lot to a number of recycling operations, which is considered a maximum and then re-test the properties defined in 13.1a. If the powder meets the acceptance criteria of this clause, every recycling step in between can also be considered acceptable.

ECSS-Q-ST-70-80_1480200

Any powder batch containing used powder shall be considered recycled powder.

## Blending

ECSS-Q-ST-70-80_1480201

          - For class 1.1, 1.2, and 2 parts, no blending of powder lots shall be permitted.

Mixing of powder lots is not permitted as traceability of powders is then lost. Opposed to this, mixing of powder batches is permitted.

ECSS-Q-ST-70-80_1480202

For class 3 parts, powders may be mixed, if it can be demonstrated that the blend has properties in accordance with requirements from clause 13.1a.

## Disposal

ECSS-Q-ST-70-80_1480203

          - Powders shall be disposed in compliance with national or European occupational health regulations.

(normative)
Preliminary Manufacturing Concept Review (PMCR) - DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 6.3b.

Purpose and objective

The aim of the AM definition phase is to converge to a preliminary manufacturing concept, allowing for an early assessment of the envisaged AM project. Conducting a feasibility study before starting the AM definition phase intends to help identifying critical aspects at an early stage. The PMCR is the formal review where the conclusions of this feasibility study are documented and presented.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480204

          - The supplier shall present the preliminary manufacturing concept, including as a minimum:

An overview of all applicable, application-specific requirements

The safety class

The selected AM end to end manufacturing process

Design allowables from a MPD (if available)

AMP (if available and verifiable)

Special remarks

None.

(normative)
Additive Manufacturing Procedure (AMP) - DRD

DRD identification

Requirement identification and source document

This DRD is called from the requirement 7.2.3a.

Purpose and objective

The purpose of the AM Procedure is to ensure that all relevant information relating to the production of each AM part, including pre-and post-processing, is documented in sufficient detail such that repeatability of the AM end to end process is given.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480205

          - The AMP shall contain the following information:

A flow chart, detailing all performed operations and their sequence from design up to final cleaning and controls, indicating the responsible stakeholder(s)

General information

Date, issue and revision number,

Powder,

AM process,

Reference to the test report in compliance with Annex D.

Equipment and facilities

Referential axis definition in compliance with clause 5.1,

Identification of the equipment, model and serial number, used to perform all processes,

Machine management system software,

Reference to procedures of all applied processes.

Reference to powder management plan in compliance with Annex I.

Reference to AM process parameter set

Shielding gas

Shield gas identification and purity,

Shield gas flow rate and direction,

Level of oxygen during the build,

Beginning, ending and duration of the shielding gas.

Level of vacuum

In case of pre-heating is applied, the temperature, and the time at temperature

Base plate

Alloy type of base plate,

Thickness of base plate,

Base plate temperature.

Type of recoater (blade, material of blade, roller, or other)

1	to item 3.(d): This includes e.g. preparatory processes, the AM process, surface treatment, heat treatment, non-destructive testing, marking and, cleaning.

2	to item 9.(b): The baseplate serves several purposes. One of them is to provide stiffness to counter-act bending forces due to the accumulation of residual stresses during the build process. High-strength materials and parts with high-volume cross sections may require thicker plates than materials with lower strength or filigree designs.

3	to item 10.: A cryptographic hash can be useful to unambiguously identify digital files as reference to AM process parameter set.

Additional requirements for various AM processes

ECSS-Q-ST-70-80_1480206

          - In addition to the requirements specified in B.2.1, the AMP for Electron Beam based Powder Bed Fusion processes shall contain as a minimum, the following information

Equipment:

Model and make,

Electron gun type.

Manufacturers’ or measured values for the beam quality parameters.

ECSS-Q-ST-70-80_1480207

In addition to the requirements specified in B.2.1, the AMP for Laser based Powder Bed Fusion processes shall contain as a minimum, the following information:

Equipment:

Type of energy source, model and make.

Special remarks

None.

(normative)
AM verification plan (AMVP) - DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 7.4.1a.

Purpose and objective

The AM verification plan is used to ensure that all relevant information related to the verification testing is documented in sufficient detail for the customer to agree on the implementation of the test programme.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480208

          - For Safety Class 1.1, 1.2, and 2: Powder characteristics (CoC or test results) including chemical composition, flow rate, and size distribution shall be annexed to this AMVP.

ECSS-Q-ST-70-80_1480209

          - The AM verification plan shall include the following information:

Tensile tests: sample type, surface finishing, criteria of acceptance

Fatigue tests: sample type, surface finishing, levels of stress for Woehler curve, stress ratio and criteria of acceptance

CT scan: strategy and criteria of acceptance

Cleanliness: method and criteria of acceptance

Specific tests: description, applicable specification and criteria of acceptance

ECSS-Q-ST-70-80_1480210

The pAMP shall be attached to the AM verification plan.

Special remarks

None.

(normative)
AM Verification Report (AMVR) – DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 7.4.4b.

Purpose and objective

The purpose of the Additive Manufacturing verification report is to ensure that all relevant information related to the results of the verification testing is documented in sufficient detail for the customer to agree on the verification.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480211

          - The verification test report shall include the following information:

            - Reference to AMP

Quantity and shape of samples

Short tests description

Test results

Analysis of results

Acceptance criteria for witness specimens

Conclusion: verification PASS or FAIL

Special remarks

None.

(normative)
Hardware Fabrication Procedure (HFP) - DRD

DRD identification

Requirement identification and source document

This DRD is called from the requirement 7.5.1b and 8.2.1a.

Purpose and objective

The purpose of the Hardware Fabrication Procedure is to define the conditions how the Additive Manufacturing Hardware has to be produced.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480212

          - The Hardware Fabrication Procedure (HFP) shall contain the following information:

Reference to AMP

Safety Class (1.1, 1.2, 2 or 3), as agreed between the design authority and the customer

The build job configuration

Reference to Prototype Verification Report

List of witness tests in accordance with clauses 8.2.3, 8.3, and 8.4

Special remarks

None.

(normative)
Hardware Production Report (HPR) - DRD

DRD identification

Requirement identification and source document

This DRD is called from the requirement 8.5a.

Purpose and objective

The purpose of the Hardware Production Report is to report the any results of performed tests on witness specimens and performed NDT.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480213

          - The Hardware Production Report (HPR) shall contain the following information:

Reference to HFP

Witness specimens test results

NDT results

Reference to the shop traveller

Reference to Non-Conformance Reports (NCRs)

Reference to Requests for Waivers (RFWs)

Special remarks

None.

(normative)
Prototype Verification Plan (PVP) - DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 7.5.1c.

Purpose and objective

The prototype verification plan is used to ensure that all relevant information is documented in sufficient detail for the customer to agree on the implementation of the test programme.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480214

          - The prototype verification plan shall include the following information:

            - NDT: strategy and criteria of acceptance

Cleanliness inspection: method and criteria of acceptance

Specific tests: description, applicable specification and criteria of acceptance

Safety Class (1.1, 1.2, 2 or 3), as agreed between the design authority and the customer

To item 3: This can include e.g.: destructive testing, mechanical testing, functional testing, and thermo-elastic distortion.

ECSS-Q-ST-70-80_1480215

The AMP shall be attached to the PVP.

ECSS-Q-ST-70-80_1480216

The PVP shall be submitted for approval by the design authority.

Special remarks

None.

(normative)
Prototype Verification Report (PVR) - DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 7.5.4b.

Purpose and objective

The purpose of the PVR is to document all relevant results of the verification testing in sufficient detail such that the customer can judge whether it has passed or failed.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480217

          - The verification test report shall include the following information:

            - Reference to AMP

Quantity and shape of samples

Quantity and shape of prototypes

Short tests description

Test results

Analysis of results

Conclusion: verification PASS or FAIL

Special remarks

None.

(normative)
Powder Management Plan (PMP) - DRD

DRD identification

Requirement identification and source document

This DRD is called from ECSS-Q-ST-70-80, requirement 10.6.1a.

Purpose and objective

The purpose of the Powder Management Plan (PMP) is to ensure that powders are procured in sufficient quality and it shall also define safe handling, storage, loading into AM machines, recycling, blending, and disposal.

Expected response

Scope and content

ECSS-Q-ST-70-80_1480218

          - The powder management plan shall specify how powders are

            - Tested,

            - Procured,

            - Safely handled,

            - Stored,

            - Loaded,

            - Recycled,

            - Blended, and

            - Disposed.

The detailed requirements are specified in clause 13.

Special remarks

ECSS-Q-ST-70-80_1480219

          - The test results shall be made available upon request.

(informative)
Template for auditing

Example of template for auditing is given in Table J-1.

: Audit template

|  | TOPIC / QUESTION | Associated requirement | Refer to | ANSWER | Associated document | Actions |
| --- | --- | --- | --- | --- | --- | --- |
| General | Company presentation |  |  |  |  |  |
| Perimeter /Restriction | Which processes are audited? |  | Introduction/ AMP |  |  |  |
|  | Which standards are used? | Clause 2 | Normative references |  |  |  |
|  | Which raw material/alloy/powder(s) is/are used? |  |  |  |  |  |
|  | Which equipment model(s) and number(s) are used? Multiple Laser System? Machine pause(s) planned? | Clause 5.3 Clause 7.7 | Multiple Laser Systems Machine pause management |  |  |  |
|  | Which design software is used? |  |  |  |  |  |
|  | Which parts are to be manufactured? Which powder/equipment is used? Which safety class is applied? Is the concept of family of parts applied? | Clause 5.2 Clause 5.4 | Family of parts Safety classes |  |  |  |
| Specification | Review of purchase specification & Contract |  |  |  |  |  |
| Verification | Is the AM definition phase well understood? Any deviations to requirements RFDs? | Clause 6 Annex A | AM definition phase PMCR |  |  |  |
|  | Is the AM verification phase well understood? Any deviations to requirements RFDs? | Clause 7 Annex B Annex C Annex D Annex E Annex F Annex G Annex H | AM verification phase AM procedure AMVP & AMVR PVP & PVR |  |  |  |
| Inputs and manufacturing documents | Are the internal AM procedures for the intrinsic process parameters compliant to Annex B? | Annex B | AM Procedure |  |  |  |
|  | Is a specific manufacturing procedure available (including a flow chart) to produce parts identified in this project? | Clause 8 Annex E | Hardware fabrication procedure Hardware production control Hardware production |  |  |  |
|  | Which processes and tests, or inspections are sub contracted? |  |  |  |  |  |
| Environment | How are the tools, used to produce these parts, controlled? |  |  |  |  |  |
|  | Is the environment and the equipment sufficient to guarantee the customer requirements? |  |  |  |  |  |
|  | How are software and its changes managed? |  |  |  |  |  |
|  | What post process treatments are used? How are these processes documented? (e.g.: part removal, mechanical, thermal, surface treatment, etc.) |  |  |  |  |  |
|  | How are oxygen / gas levels managed in the machines? |  |  |  |  |  |
|  | How is test and inspection equipment managed? (for controls, tests, dimensional measurement, etc.) |  |  |  |  |  |
|  | How is cleanliness after all post process operations managed? |  |  |  |  |  |
|  | Has an AM supervisor been appointed? | Clause 9.2 | AM supervisor |  |  |  |
| Personnel | How are AM operators trained? | Clause 9.3 | AM operators |  |  |  |
|  | How are AM inspectors trained? | Clause 9.4 | AM inspectors |  |  |  |
|  | What is the validity period of the certificates? |  |  |  |  |  |
|  | What are the conditions for maintaining the certification? |  |  |  |  |  |
|  | Are the training and certificates managed internally or externally? |  |  |  |  |  |
|  | Is a skills matrix available and is there redundancy for AM operators and AM inspectors? |  |  |  |  |  |
|  | Are the conditions for facilities understood and met? | Clause 10.2 | Conditions for facilities |  |  |  |
| Equipment and facilities | Are the requirements for Laser Beam calibration understood and met? | Clause 10.3 | Laser Beam calibration |  |  |  |
|  | Are the requirements for electron beam calibration understood and met? | Clause 10.4 | EB calibration |  |  |  |
|  | Are the requirements for maintenance and repair (laser based machine) understood and met? | Clause 10.5.1 Clause 10.5.3 Clause 7.6 | Maintenance and Repair (laser based machine) Re-Verification |  |  |  |
|  | Are the requirements for maintenance and repair (EB based machine) understood and met? | Clause 10.5.2 Clause 10.5.3 Clause 7.6 | Maintenance and Repair (EB based machine) Re-verification |  |  |  |
|  | Are the requirements for cleaning the machine understood and met? (e.g.: How is a change of powder in the machine performed?) | Clause 10.6.4 | Cleaning of machine |  |  |  |
| Materials and Consumables | Which powder properties are tested and how is this done? | Clause 10.6.1 Annex 13.1 | Management of powders Testing |  |  |  |
|  | Is a CoC available for raw material / purchasing specification? | Clause 10.6.1 Clause 13.2 | Management of powders Procurement |  |  |  |
|  | How is the incoming inspection performed? | Clause 10.6.1 Clause 13.1 | Management of powders Testing |  |  |  |
|  | How is powder traceability managed? |  |  |  |  |  |
|  | How is the recycling of powders managed? | Clause 10.6.1 Clause 13.6 | Management of powders Recycling |  |  |  |
|  | How is the powder quality ensured after several recycling steps? | Clause 10.6.1 Clause 13.7 | Management of powders Blending |  |  |  |
|  | How are the powder storage conditions managed? (e.g.: protection against humidity and oxidation, etc.) | Clause 10.6.1 Clause 13.4 | Management of powders Storage |  |  |  |
|  | Is there a drying process for powder before production? If yes, how is it managed? |  |  |  |  |  |
|  | Are the requirements for gas management understood and met? | Clause 10.6.3 | Gases |  |  |  |
|  | Are the requirements for tooling understood and met? | Clause 10.6.2 | Tooling |  |  |  |
| Non-destructive testing | Are the requirements for NDI and density understood and can they be met? | Clause 12.3 and 12.4 | NDI & density |  |  |  |
| Destructive testing | Are the requirements or recommendations for Destructive testing understood? | Clause 12.5 | Destructive testing |  |  |  |
| Quality assurance & Manufacturing | Industrial documentation | Clause 11.2 Clause 11.4.1 Clause 11.4.2 Clause 11.6 Annex B | Maintenance of AMP Witness sample Documentation of manufacturing EIDP AM procedure |  |  |  |
|  | Are the requirements for SPC understood and met? | Clause 11.3 | SPC |  |  |  |
|  | Process Monitoring NC and delays management | Clause 11.4.3 |  |  |  |  |

Special remarks

None.

(informative)
Example of a Materials Properties Database (MPD)

Example of Materials Properties Database (MPD) is given in Table K-1.

: Example of a Materials Properties Database

|  | Mechanical properties |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| AMP reference | UTS | YS (or PS) | Elongation | Young’s Modulus E | Other | Density |

Bibliography

| ECSS-S-ST-00 | ECSS system – Description, implementation and general requirements |
| --- | --- |
| ECSS-E-ST-32-01 | Space engineering - Fracture control |
| ASTM B212:2017 | Standard Test Method for Apparent Density of Free-Flowing Metal Powders Using the Hall Flowmeter Funnel |
| ASTM B213:2020 | Standard Test Methods for Flow Rate of Metal Powders Using the Hall Flowmeter Funnel |
| ASTM B214:2016 | Standard Test Method for Sieve Analysis of Metal Powders |
| ASTM B527:2020 | Standard Test Method for Determination of Tap Density of Metallic Powders and Compounds |
| ASTM B822:2017 | Standard Test Method for Particle Size Distribution of Metal Powders and Related Compounds by Light Scattering |
| ASTM B923:2020 | Standard Test Method for Metal Powder Skeletal Density by Helium or Nitrogen Pycnometry |
| ASTM B962:2017 | Standard Test Methods for Density of Compacted or Sintered Powder Metallurgy (PM) Products Using Archimedes’ Principle. |
| ASTM B964:2016 | Standard Test Methods for Flow Rate of Metal Powders Using the Carney Funnel |
| ASTM E203:2016 | Standard Test Method for Water Using Volumetric Karl Fischer Titration |
| ASTM E1131:2020 | Standard Test Method for Compositional Analysis by Thermogravimetry |
| ASTM E1409:2013 | Standard Test Method for Determination of Oxygen and Nitrogen in Titanium and Titanium Alloys by Inert Gas Fusion |
| ASTM E1447:2016 | Standard Test Method for Determination of Hydrogen in Titanium and Titanium Alloys by Inert Gas Fusion Thermal Conductivity/Infrared Detection Method |
| ASTM E1508:2019 | Standard Guide for Quantitative Analysis by Energy-Dispersive Spectroscopy |
| ASTM E1941:2016 | Standard Test Method for Determination of Carbon in Refractory and Reactive Metals and Their Alloys by Combustion Analysis |
| ASTM E2371:2013 | Standard Test Method for Analysis of Titanium and Titanium Alloys by Direct Current Plasma and Inductively Coupled Plasma Atomic Emission Spectrometry (Performance-Based Test Methodology) |
| ASTM E3061:2017 | Standard Test Method for Analysis of Aluminum and Aluminum Alloys by Inductively Coupled Plasma Atomic Emission Spectrometry (Performance Based Method) |
| ASTM E3166:2020 | Standard Guide for Nondestructive Examination of Metal Additively Manufactured Aerospace Parts After Build |
| ASTM F2924:2014 | Standard Specification for Additive Manufacturing Titanium-6 Aluminum-4 Vanadium with Powder Bed Fusion |
| ASTM F3001:2014 | Standard Specification for Additive Manufacturing Titanium-6 Aluminum-4 Vanadium ELI (Extra Low Interstitial) with Powder Bed Fusion |
| ASTM F3055:2014 | Standard Specification for Additive Manufacturing Nickel Alloy (UNS N07718) with Powder Bed Fusion |
| ASTM F3056:2014 | Standard Specification for Additive Manufacturing Nickel Alloy (UNS N06625) with Powder Bed Fusion |
| ASTM F3184:2016 | Standard Specification for Additive Manufacturing Stainless Steel Alloy (UNS S31603) with Powder Bed Fusion |
| ASTM F3318:2018 | Standard for Additive Manufacturing – Finished Part Properties – Specification for AlSi10Mg with Powder Bed Fusion – Laser Beam |
| EN ISO 3369:2010 | Impermeable sintered metal materials and hardmetals - Determination of density |
| ISO 760:1978 | Determination of water - Karl Fischer method (General method) |
| ISO 3923-1:2018 | Metallic powders - Determination of apparent density - Part 1: Funnel method |
| ISO 3953:2011 | Metallic powders - Determination of tap density |
| ISO 4324:1977 | Surface active agents - Powders and granules - Measurement of the angle of repose |
| ISO 4490:2018 | Metallic powders - Determination of flow rate by means of a calibrated funnel (Hall flowmeter) |
| ISO 4491-4:2019 | Metallic powders - Determination of oxygen content by reduction methods - Part 4: Total oxygen by reduction-extraction |
| ISO 4497:2020 | Metallic powders - Determination of particle size by dry sieving |
| ISO 13320:2020 | Particle size analysis - Laser diffraction methods |
| ISO 13322:2014 | Particle size analysis - Image analysis methods - Part 1: Static image analysis methods |
| ISO 22309:2011 | Microbeam analysis - Quantitative analysis using energy-dispersive spectrometry (EDS) for elements with an atomic number of 11 (Na) or above |
| NASA MSFC 3717:2017 | MSFC Technical standard specification for control and qualification of laser powder bed fusion metallurgical processes |
| MMPDS-14:2019 | Metallic Materials Properties Development and Standardisation |